CHANGES TO HBP SPECIFICATIONS

(Gyratory Compaction Angle & Air Voids)

I.	The following changes will be required for all HBP placed after January 1, 2003:

- Change gyratory compaction angle for all gyratory compactors to 1.25 degrees.

1.	This will allow CDOT to comply with the specifications being used by all other states and permit comparison of results with national data.

2.	Changing the gyratory angle from 1.20 to 1.25 degrees will increase the compactive effort used in the mix design It has been determined that changing the angle to 1.25 degrees will reduce the air voids by approximately 0.3% for a given asphalt cement content. This means a mix designed using a gyratory angle of 1.25 degrees will contain approximately 0.1% less asphalt cement than one designed with a gyratory angle of 1.20 degrees.

B.	The CDOT Form # 43 will establish construction targets for Asphalt Cement and all mix properties at Air Voids 1.0% below mix design optimum.

- The data collected from the In-Place Voids study conducted by the Research Branch indicates that CDOT’s existing asphalt pavements are too stiff and do not contain the optimum amount of Asphalt Cement to ensure long term performance. (Please see Research Report Number CDOT-DTD-R-2002-11 for more information.)

- Establishing the air voids target at 1.0% below the target values from the optimum determined in the mix design will add approximately 0.3% asphalt cement to the mix.

C.	Summary of the Changes to HBP

Since the increase in the gyratory angle from 1.20 to 1.25 degrees will reduce the asphalt cement by approximately 0.1% and establishing the air voids 1.0% below the mix design optimum will increase the asphalt cement content by about 0.3%, we anticipate a net increase in asphalt content for all CDOT mixes of approximately 0.2%.

- Construction Contract Administration Issues for Projects With Asphalt Pavement.

There are four categories of projects that will be affected by these changes.

A.	Projects that have not been advertised.

A Project Special Provision and Standard Special Provision will be immediately issued to implement the above referenced changes and will be included in these projects.

No field changes will be required.

- Projects that are under advertisement.

The Project special Provision and Standard Special Provision implementing these changes will be added to these projects with a revision under advertisement. (The new Special Provisions: Project Special Provision: Rev. of Section 403 – HBP and Standard Special Provision: Rev. of Sections 105 and 106 – Quality of HBP are included with this Bulletin.)

The Project Manager will prepare and issue the revision under advertisement

C.	Projects that have been advertised and bids opened, but construction has not commenced.

- Projects that do not have an approved Mix Design.

The Project Engineer will execute a Change Order (MCR/CMO) to incorporate the Project Special Provision and Standard Special Provision. (The new Special Provisions: Project Special Provision: Rev. of Section 403 – HBP and Standard Special Provision: Rev. of Sections 105 and 106 – Quality of HBP are included with this Bulletin.)

The Change Order will create a Force Account Pay Item for additional asphalt cement. The Contractor will furnish a gyratory mix design with a 1.25-degree angle. The amount of additional asphalt cement that will be paid will be calculated as follows:

% Additional asphalt cement to be paid = %AC1 – AC2 – 0.1 % =

%AC1 = 	asphalt content after 1% shift in target air voids from optimum air voids

%AC2 = 	% asphalt cement at optimum air voids

0.1% = 	approximate amount of asphalt cement reduction between gyratory compaction at 1.20 and 1.25 angle.

Contractor will furnish a certified invoice for the asphalt cement and the15% mark up for materials will be paid.

When binder is paid for paid separately, there will be no Force Account Pay Item for additional AC.

- Projects that have an approved Mix Design with a gyratory angle of 1.20 degrees.

The Project Engineer will execute a Change Order (MCR/CMO) to incorporate the Project special Provision and Standard Special Provision. (The new Special Provisions: Project Special Provision: Rev. of Section 403 – HBP and Standard Special Provision: Rev. of Sections 105 and 106 – Quality of HBP are included with this Bulletin.) The Change Order will require the Contractor to run a new mix design with a gyratory angle of 1.25 degrees. The Change Order will also create Force Account Pay Items for the cost of the new Mix Design and the additional asphalt cement if any required at the production voids target 1% below the new mix design optimum.

Contractor will furnish a certified invoice for the asphalt cement and mix design and the15% mark up for materials will be paid on the asphalt cement.

When binder is paid for paid separately, there will be no Force Account Pay Item for additional AC.

  - Projects that have been previously started and are not complete.

The Project Engineer will execute a Change Order (MCR/CMO) to incorporate the Project Special Provision and Standard Special Provision. (The new Special Provisions: Project Special Provision: Rev. of Section 403 – HBP and Standard Special Provision: Rev. of Sections 105 and 106 – Quality of HBP are included with this Bulletin.)

The Change Order will require the Contractor to run a new mix design with a gyratory angle of 1.25 degrees. The Change Order will also create Force Account Pay Items for the Mix Design and the additional asphalt cement if any required at the production voids target 1% below the new mix design optimum.

Contractor will furnish a certified invoice for the asphalt cement and mix design and the15% mark up for materials will be paid on the asphalt cement.

When binder is paid for paid separately, there will be no Force Account Pay Item for additional AC.

If you have questions or we can assist you in anyway, please call your Project Development Branch Area Engineer. Jim Zufall 303-757-9326 or Hal Toland 303-757-9595.