Asphalt Pavement Workability

The Colorado Department of Transportation (CDOT), The Colorado Asphalt Paving Association (CAPA), the Colorado Asphalt Paving Industry and private consultants have formed a taskforce called the “Workability Evaluation Team” (WET) to investigate mix workability problems on asphalt paving projects in Colorado.

The WET was established to investigate projects where obtaining the required compaction is difficult or impossible because the asphalt pavement exhibits signs of shoving; tenderness, and tearing. These problems are being called "mix workability" problems and are the primary focus of the WET. The WET will gather information on workability problems to minimize them on future projects. The primary goal of the effort is not to solve individual project problems, but to gather information on all workability problem projects and improve existing project materials and construction guidelines.

It will be assumed that a mix workability problem exists when the Project Engineer and the Contractor’s Superintendent agree that there is an unusual problem when attempting to obtain compaction.

The Project Engineer or Contractor’s Superintendent should immediately contact one of the co-chairman of the WET when they agree there is a problem:

Jim Fife, Western Colorado Testing:

Office: 	(970) 241-7700   Cellular: (970) 260-0953

Bill Schiebel, CDOT Asphalt Pavement Program:

Office:	(303) 757-9235   Cellular (720) 289-1377

The WET will attempt to visit the construction project during the next full day of paving. The WET will coordinate with and be accompanied by the appropriate Region personnel. At a minimum, the Construction Project Engineer and the Region Materials Engineer will be consulted prior to project evaluation. The WET will ensure that the binder supplier and Contractor are notified of the WET visit to the project.

The WET developed the attached protocol for investigating mix workability problems.

The WET will use the attached Field sheets to record information from each individual project.