Sample Project Special Provision: 601aebz

1/9/09

REVISION OF SECTION 601

AIR ENTRAINED BZ CONCRETE

Section 601 of the Standard Specifications is hereby revised for this project as follows:

In subsection 601.02, delete Class BZ and replace with the following:

Class BZ concrete is concrete for drilled piers.  Additional requirements are:  Entrained air is not required unless specified in the Contract.  When entrained air is specified in the Contract, the air content shall be 5-8 percent.  High range water reducers may be added to obtain desired slump and retardation.  Slump shall be a minimum of 5 inches and a maximum of 8 inches.  The concrete mix shall be made with AASHTO M 43 size No. 67, No. 7 or No. 8 coarse aggregate. Approved fly ash may be substituted for portland cement up to a maximum of 20 percent Class C or 30 percent Class F by weight of total cementitious.

Subsection 601.05 shall include the following:

When entrained air is specified in the Contract for Class BZ concrete, an air entraining admixture may be added to an approved Class BZ.  A new trial mix will not be required.

INSTRUCTIONS TO DESIGNERS:

The Designer will add this revision when specifying entrained air in Class BZ concrete