Sample project special: 608dw

06-29-06

1

REVISION OF SECTION 608

DETECTABLE WARNINGS

Section 608 of the Standard Specifications is hereby revised for this project as follows:

Subsection 608.01 shall include the following:

This work includes the installation of detectable warnings on concrete curb ramps at the locations shown on the plans and in accordance with the plans.

Subsection 608.02 shall include the following:

Detectable warnings on curb ramps shall be truncated domes of the dimensions shown on the plans.  Domes shall be prefabricated by the manufacturer as a pattern on concrete or masonry pavers.

Pavers shall meet all Americans with Disabilities Act (ADA) requirements for truncated domes, and when installed, shall be capable of producing the pattern of domes as shown on the plans.

Pavers shall meet the requirements of ASTM C 902 or ASTM C 936.

Alternate materials may be used, if pre-approved by the Engineer.   The Contractor shall submit a sample of the product, the name of the selected supplier, and documentation that the product meets all contrast requirements and will be fully compatible with the curb ramp surface to the Engineer for approval prior to start of work.  Known vendors of alternate products include but are not limited to the following:

| Vendor Name | Product | Phone Numbers |
| --- | --- | --- |
| Engineered Plastics, Inc. | Armor-Tile Cast-in-Place or Modular Paver Detectable Warning System | 800-682-2525 |
| TMA Construction Supply | CAST in TACT Warning Panels | 303-295-6050 |
| East Jordan Iron Works, Inc. | Truncated Dome Plates | 800-626-4653 |

The domes and the underlying surface shall have a minimum of 70% contrast with the light reflectivity of the adjoining surface.  The contrast shall be verified using the following equation:

Where  = Light Reflectance Value (LRV) of the lighter area

= LRV of the darker area

Absolute black and white will not be permitted.

Sample project special: 608dw

06-29-06

2

REVISION OF SECTION 608

DETECTABLE WARNINGS

The contrast shall be achieved by adding pigment during the fabrication of the paver.  Prior to start of work, the Contractor shall submit appropriate documentation from the manufacturer verifying that the contrast has been met, along with a sample paver, to the Engineer for approval.

Bedding and joint sand shall be free of deleterious or foreign matter.  The sand shall be natural or manufactured from crushed rock.  Limestone screenings or stone dust shall not be used.  Sand for bedding material shall conform to ASTM C 33.  Sand that is to be placed between joints shall conform to ASTM C 144.

Subsection 608.03 shall include the following:

(g)	Detectable Warnings.  Pre-fabricated pavers for detectable warnings shall be brought to the site in steel banded, plastic banded or plastic wrapped cubes capable of being transported by a fork lift or clamp lift.  Pavers shall be carefully removed and stacked in a manner which results in the least amount of damage.  All pavers that are damaged during transport or delivery will be rejected and shall be replaced at the Contractor’s expense.  Minor cracks or chipping due to transport and handling that do not interfere with the structural integrity of the paver or the overall pattern of truncated domes will not be deemed as grounds for rejection.

The Contractor shall spread the bedding sand evenly in the area defined and shall screed the sand to an appropriate embedment depth as shown on the plans or as directed by the Engineer.  Sufficient sand should be placed to stay ahead of laid pavers

Pavers shall be placed in a running bond pattern.  Pavers shall be installed such that the base of the truncated dome is at the same elevation as the adjoining surface, allowing for a smooth transition between the curb ramp and the detectable warning.

When cut pavers are required to fill gaps between the pavers and the edge of concrete, the Contractor shall bevel portions of the truncated domes at a 45-degree angle to create a smooth transition between the partial dome and the curb ramp surface.  Unless otherwise directed by the Engineer, pavers shall be cut and installed in such a manner that the domes on the cut sections will not significantly impact the overall pattern of the truncated domes.

The Contractor shall use a plate vibrator to embed the pavers into the sand.  The size and type of plate vibrator shall be in accordance with manufacturer’s recommendations, or as directed by the Engineer.  All pavers that are damaged during embedment shall be replaced at the Contractor’s expense.

Joint spacing between paver units shall be in accordance with the manufacturer’s recommendations, or as approved by the Engineer.  Joints shall be filled completely with joint sand.  Excess sand shall be removed by sweeping.

(h)	Alternate products.   Alternate materials shall be installed in accordance with manufacturer’s recommendations.

Sample project special: 608dw

06-29-06

3

REVISION OF SECTION 608

DETECTABLE WARNINGS

The concrete surface to which alternate materials are to be applied shall be prepared in accordance with manufacturer’s recommendations. Material requirements, color and application shall be in accordance with manufacturer’s recommendations and as approved by the Engineer.

Subsection 608.05 shall include the following:

Detectable warnings on curb ramps, including sand, pavers, alternate materials, and all other work and materials necessary for fabrication, transport, and installation will not be measured and paid for separately, but shall be included in the work.