#### July 3, 2008

## Revision of Section 105

### Conformity TO THE CONTRACT OF

### SUPERPAVE PERFORMANCE GRADED BINDERS

##### NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction.  It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions for its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions issued unless such use is first approved by the Standards and Specifications Unit of the Project Development Branch.  The instructions for use on CDOT construction projects appear below.

Other agencies which use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use this standard special provision on projects with HMA having Superpave PG binders.

July 3, 2008

1

REVISION OF SECTION 105

CONFORMITY TO THE CONTRACT OF

SUPERPAVE PERFORMANCE GRADED BINDERS

Section 105 of the Standard Specifications is hereby revised for this project as follows:

Delete subsection 105.04 and replace with the following:

105.04 Conformity to the Contract of Superpave Performance Graded Binders.  Asphalt binders will be price reduced according to the following if the requirements of subsection 702.01 are not met:

TABLE OF PERFORMANCE GRADED BINDER LIMITS

| Property | Specification | Compliance Limit for Price Reduction of 0% | Rejection Limit, Price Reduction = 25% |
| --- | --- | --- | --- |
| G*sin (delta) of RTFO Residue | 2.20 Min | 1.87 Min | < 1.53 |
| Slope (m-value) of the Creep Curve at Low Grade Temperature + 10° C. | 0.300 Min | 0.295 Min | < 0.266 |
| Stiffness of the PAV Residue at Low Grade Temperature + 10° C, (Mpa) | 300 Max | 311 Max | >355 |

The price reduction will be 25 percent at the rejection limit.  Between the compliance limit and the rejection limit, the price reduction will be calculated as follows:

PR = 25 ●    CL – test value

CL – RL

Where:	PR = Price Reduction

CL = Compliance Limit

RL = Rejection Limit

- The price reductions will be cumulative if more than one PG binder property specified in the Table of Performance Graded Binder Limits is out of specification, resulting in P(total).  When binder is included in the contract unit price for HMA, the price reduction will be calculated as follows:

Amount of Reduction = [P(total)] ● [(1/100) ●  (Invoice Price for PG Binder)]

When the binder is paid for separately, the total price reduction will be calculated as follows:

Amount of Reduction =  [P(total)] ● [(1/100) ● (Contract Unit Price for PG Binder)]

- Price reductions based on the “F” factors in the Table of Price Reduction Factors described in subsection 105.03 will be in addition to the PG binder price reductions.  Other binder requirements listed in the Table of Performance Graded Binder Limits but not price reduced in subsections 105.03 or 105.04 may be tested, but will not be considered for price reduction calculations.  However, the Contractor will not be allowed to continue to produce mix with out of specification PG binder.  If two consecutive samples fail to meet all requirements listed in the Table of Performance Graded Binder Limits, the Contractor shall take corrective action before being allowed to continue production of Hot Mix Asphalt.  If proper corrective measures cannot

July 3, 2008

2

REVISION OF SECTION 105

CONFORMITY TO THE CONTRACT OF

SUPERPAVE PERFORMANCE GRADED BINDERS

be readily determined, the Engineer will suspend the use of such material until the Engineer can determine from laboratory tests that the Contractor can provide material that is in compliance with the Table of Performance Graded Binder Limits.

The Contractor will not have the option of accepting a price reduction in lieu of producing specification material.  Continued production of non-specification material will not be permitted.  Material which is obviously defective may be isolated and rejected without regard to sampling sequence or location within a lot.