# October 21, 2010

REVISION OF SECTION 401

COMPACTION PAVEMENT TEST SECTION (CTS)

**NOTICE**

This is a standard special provision that revises or modifies CDOT’s *Standard Specifications for Road and Bridge Construction.* It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions for its use on CDOT construction projects. It is to be used as written without change. Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by the Standards and Specifications Unit of Project Development. The instructions for use on CDOT construction projects appear below.

Other agencies which use the *Standard Specifications for Road and Bridge Construction* to administer construction projects may use this special provision as appropriate and at their own risk.

**Instructions for use on CDOT construction projects:**

Use this standard special provision on projects having hot mix asphalt.

October 21, 2010

REVISION OF SECTION 401

COMPACTION PAVEMENT TEST SECTION (CTS)

Section 401 of the Standard Specifications is hereby revised for this project as follows:

In subsection 401.17, delete the fourteenth paragraph and replace with the following:

Two sets of random cores shall be taken within the last 200 tons of the CTS. Each set shall consist of a minimum of seven random corings. The Engineer will determine the coring locations using a stratified random sampling process. The locations of these cores will be such that one set can serve as a duplicate of the other. One set of these cores shall be immediately submitted to the Engineer. This set will be used for determining acceptance of the CTS and determining density correction factors for nuclear density equipment. Densities of the random samples will be determined by cores according to CP 44. Density correction factors for nuclear density equipment will be determined according to CP 81. Coring shall be performed under CDOT observation. Coring will not be measured and paid for separately but shall be included in the work. For SMA, a CTS is not used. The Contractor shall follow the requirements for the demonstration control strip in accordance with the Revision of Section 403, Stone Matrix Asphalt Pavement.