July 30, 2009

REVISION OF SECTION 401

PREPARATION OF AGGREGATES

NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction.  It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions for its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by CDOT’s Standards and Specifications Unit.  The instructions for use on CDOT construction projects appear below.

Other agencies which use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use this standard special provision on all projects having any grade of hot mix asphalt.

July 30, 2009

REVISION OF SECTION 401

PREPARATION OF AGGREGATES

Section 401 of the Standard Specifications is hereby revised for this project as follows:

In subsection 401.14, second paragraph, delete item (2) and replace it with the following:

- Dry Lime Added to Wet Aggregate. The dry hydrated lime shall be added to aggregate wetted a minimum of 2 percent above the surface saturated dry condition (SSD) of the blended aggregate as shown on the Form 43, and then thoroughly mixed in an approved pug mill. The Engineer will not require the Contractor to go above 5 percent total moisture, although the Contractor may elect to do so if the added water is necessary to meet the minimum Lottman specification (See Table 401-2.).

The Contractor may request that the 2 percent above SSD requirement be waived, provided the requirements of CPL 5150 have been met.  If the HMA fails to meet the minimum TSR requirements defined in Table 401-2 at any point during production, the Contractor shall immediately be required to add the minimum amount of moisture as defined above.