April 11, 2008

REVISION OF SECTION 409

COVER COAT MATERIAL

NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction  It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions for its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by CDOT’s Standards and Specifications Unit.  The instructions for use on CDOT construction projects appear below.

Other agencies which use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use in all projects having cover coat material.

April 11, 2008

Revision of Section 409

Cover Coat Material

Section 409 of the Standard Specifications is hereby revised for this project as follows:

In subsection 409.08, delete the second and fifth paragraphs, and replace with the following:

The cover coat material shall be moistened prior to spreading with a sufficient amount of water to reduce the dust coating of the aggregate.  The cover coat material shall not contain free moisture as evidenced by drain down in the delivery truck bed.

A fog coat shall be applied at the rate of 0.11 ± 0.04 gallon per square yard of diluted emulsion when directed. The fog coat shall have a 3:2 emulsion to water dilution rate. The application rate and the dilution rate may be changed by the Engineer.