July 30, 2009

REVISION OF SECTION 711

CURING MATERIALS

NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction.  It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions for its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by CDOT’s Standards and Specifications Unit.  The instructions for use on CDOT construction projects appear below.

Other agencies which use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use this standard special provision on all projects having any type of portland cement concrete construction.

July 30, 2009

REVISION OF SECTION 711

CURING MATERIALS

Section 711 of the Standard Specifications is hereby revised for this project as follows:

Delete subsection 711.01 and replace it with the following:

711.01 Curing Materials. Curing materials shall conform to the following requirements:

Burlap Cloth made from Jute or Kenaf 		AASHTO M 182

Liquid Membrane-Forming Compounds

for Curing Concrete				AASHTO M 148

Sheet Materials for Curing Concrete 		AASHTO M 171*

*Only the performance requirements of AASHTO M171 shall apply.

Straw used for curing shall consist of threshed straw of oats, barley, wheat, or rye.  Clean field or marsh hay may be substituted for straw when approved by the Engineer.  Old dry straw or hay which breaks readily in the spreading process will not be accepted.