July 30, 2009

REVISION OF SECTION 713

GLASS BEADS FOR TRAFFIC MARKING

NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction.  It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions for its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by CDOT’s Standards and Specifications Unit.  The instructions for use on CDOT construction projects appear below.

Other agencies which use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use this standard special provision on all projects having any type of pavement marking.

July 30, 2009

REVISION OF SECTION 713

GLASS BEADS FOR TRAFFIC MARKING

Section 713 of the Standard Specifications is hereby revised for this project as follows:

Subsection 713.08 shall include the following:

Glass beads used for any type of pavement marking shall not contain more than 75 parts per million (ppm) Arsenic, 75 ppm Antimony and 100 ppm Lead.