### January 16, 2004

REVISION OF SECTIONS 401

# DENSITY PROFILES

#### NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction.  It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions regarding its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by the Standards and Specifications Unit of the Project Development Branch.  The instructions for use on CDOT construction projects appear below.

Other agencies that use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use this standard special provision on projects having 5000 or more tons of hot bituminous pavement.

January 16, 2004

REVISION OF SECTION 401

Density Profiles

Section 401 of the Standard Specifications is hereby revised for this project as follows:

Subsection 401.16, shall include the following:

The Contractor shall conduct a minimum of five density profile measurements, at the Contractors expense.  Density Profiles are described below and shown at the bottom of the “HBP Density Profile Data Sheet”.  The Engineer will designate and mark the density profile locations. Data shall be recorded on the “HBP Density Profile Data Sheet” and the data sheet shall be given to the Engineer within two days of testing.  Density Profiles shall include one Paver profile and one Control profile.  The three additional profiles shall be of visible or strip segregation, if available. If three locations of visible or strip segregation are not available, Stops will be profiled.  If there are insufficient Stops, then additional Controls shall be profiled to bring the total profiles to five. The Contractor shall not make additional stops only for the purpose of creating additional locations for profiling. Pavement densities for the profile shall be determined in accordance with CP 81, except that only one, 1-minute count shall be taken at each test location.

The five types of density profiles shall be conducted as described below.  The name of each type of profile is in parentheses.  The Contractor shall record the type of profile on the HBP Density Profile Data Sheet.

- Hidden paver segregation possible (Paver):  Segregation caused by the paver may be detected by a transverse density profile with tests approximately every foot, starting and finishing one foot in from the edge of the paving pass.  One additional reading shall be taken at each of the three following locations: The mat locations corresponding to the outside ends of the paver’s slat conveyors and the auger box.

- Control profile (Control):  Control profiles will be located where both of the following conditions prevail: There is no visible segregation and the paver has not stopped.  Control profiles will be longitudinal, with eleven tests located approximately five feet apart.  These will provide density profile results for non-segregated pavement.

- Where the paver stops (Stop):  The paver shall have been in stop condition for at least two minutes to be considered a “Stop”.  Profiling shall start 25 feet before the screed location when the paver stopped and proceed in the direction of paving for 50 feet.  Eleven density tests shall be conducted at a spacing of approximately 5 feet apart.    The profile should be located at least one foot in from the edge of the paving pass.  The Contractor shall record the duration of the Stop on the HBP Density Profile Data Sheet. At least one reading at a Stop location shall be between the rollers and the screed.  The pavement temperature at each density testing location within the Stop location profile shall also be recorded at the time paving resumes, with either an infrared sensor or thermometer.

- Where there is visible segregation (Visible): Eleven tests at locations approximately five feet apart and along the centerline shall be conducted, beginning 10 feet prior to the start of visible segregation and proceeding through the most severe or longest portion of the visible segregation.

- Narrow strip of longitudinal segregation (Strip):  The Contractor shall conduct eleven tests at locations approximately five feet apart, starting two feet to the right of the strip of segregation and ending approximately two feet to the left of the strip.