<<403hbp>>

Work Sheet, page 1 of 4

January 16, 2004

REVISION OF SECTION 403

HOT BITUMINOUS PAVEMENT

Section 403 of the Standard Specifications is hereby revised for this project as follows:

Subsection 403.02 shall include the following:

The design mix for hot bituminous pavement shall conform to the following:

@ TABLE 403-1

| Property | Test Method | Value For Grading |
| --- | --- | --- |
|  |  | x S( ) | x SG( ) | x SX( ) | x Patching |
| Air Voids, percent at: N (initial) [for information only] N (design) | CPL 5115 | 3.5 – 4.5 | 3.5 – 4.5 | 3.5 – 4.5 | 3.5 – 4.5 |
| Lab Compaction (Revolutions): N (initial) [for information only] N (design) | CPL 5115 | ( | ( | ( | ( |
| Stability, minimum | CPL 5106 |  |  |  |  |
| Aggregate Retained on the 4.75 mm (No. 4) Sieve with at least 2 Mechanically Induced fractured faces, % minimum | CP 45 | ( | ( | ( | ( |
| Accelerated Moisture Sus-ceptibility Tensile Strength Ratio (Lottman), minimum | CPL 5109 Method B | 80 | 80 | 80 | 80 |
| Minimum Dry Split Tensile Strength, kPa (psi) | CPL 5109 Method B | 205 (30) | 205 (30) | 205 (30) | 205 (30) |
| Grade of Asphalt Cement, Top Layer |  | PG___ | PG___ | PG___ | PG___ |
| Grade of Asphalt Cement, Layers below Top |  | PG___ | PG___ | PG___ | PG___ |
| Voids in the Mineral Aggregate (VMA) % minimum | CP 48 | See Table 403-2 | See Table 403-2 | See Table 403-2 | See Table 403-2 |
| Voids Filled with Asphalt (VFA), % | AI MS-2 | ( | ( | ( | ( |
| Dust to Asphalt Ratio Fine Gradation Coarse Gradation | CP 50 | 0.6 – 1.2 0.8 – 1.6 | 0.6 – 1.2 0.8 – 1.6 | 0.6 – 1.2 0.8 – 1.6 | 0.6 – 1.2 0.8 – 1.6 |

Note:	AI MS-2 = Asphalt Institute Manual Series 2

Note:	The current version of CPL 5115 is available from the Region Materials Engineer.

Note:	Mixes with gradations having less than 40% passing the 4.75 mm (No. 4) sieve shall be approached with caution because of constructability problems.

Note:	Gradations for mixes with a nominal maximum aggregate size of one-inch or larger are considered a coarse gradation if they pass below the maximum density line at the #4 screen.

Gradations for mixes with a nominal maximum aggregate size of ¾ inch or smaller are considered a coarse gradation if they pass below the maximum density line at the #8 screen.

All mix designs shall be run with a gyratory compaction angle of 1.25 degrees and properties must satisfy Table 403-1.  CDOT Form #43 will establish construction targets for Asphalt Cement and all mix properties at Air Voids up to 1.0% below the mix design optimum.

Work Sheet, page 2 of 4

January 16, 2004

-2-

REVISION OF SECTION 403

HOT BITUMINOUS PAVEMENT

TABLE 403-2

| Minimum Voids in the Mineral Aggregate (VMA) |
| --- |
| Nominal Maximum Size*, mm (inches) | ***Design Air Voids ** |
|  | 3.5% | 4.0% | 4.5% |
| 37.5 (1½) | 11.6 | 11.7 | 11.8 |
| 25.0 (1) | 12.6 | 12.7 | 12.8 |
| 19.0 (¾) | 13.6 | 13.7 | 13.8 |
| 12.5 (½) | 14.6 | 14.7 | 14.8 |
| 9.5 (⅜) | 15.6 | 15.7 | 15.8 |

* The Nominal Maximum Size is defined as one sieve larger than the first sieve to retain 			more than 10%.

** Interpolate specified VMA values for design air voids between those listed.

***Extrapolate specified VMA values for production air voids beyond those listed.

The Contractor shall prepare a quality control plan outlining the steps taken to minimize segregation of HBP. This plan shall be submitted to the Engineer and approved prior to beginning the paving operations.  When the Engineer determines that segregation is unacceptable, the paving shall stop and the cause of segregation shall be corrected before paving operations will be allowed to resume.

#The hot bituminous pavement shall not contain any reclaimed asphalt pavement.

&Hot bituminous pavement for patching shall conform to the gradation requirements for Hot Bituminous Pavement (Grading    ).

Work Sheet, Sheet 3 of 4

January 16, 2004

-3-

REVISION OF SECTION 403

HOT BITUMINOUS PAVEMENT

%A minimum of one percent hydrated lime by mass (weight) of the combined aggregate shall be added to the aggregate for all hot bituminous pavement.

☻Acceptance samples shall be taken                 .

Subsection 403.03 shall include the following:

+The Contractor shall use an approved anti-stripping additive.  The amount of additive used shall be a minimum of 0.5% by mass (weight) of the asphalt cement.  The additive shall be added at the refinery or at the hot plant.  If liquid anti-stripping additive is added at the plant, an approved in-line blender must be used.  The blender shall be in the line from the storage tank to the drier drum or pugmill.  The blender shall apply sufficient mixing action to thoroughly mix the asphalt cement and anti-stripping additive.

yThe Contractor shall construct the work such that all roadway pavement placed prior to the time paving operations end for the year, shall be completed to the full thickness required by the plans.  The Contractor's Progress Schedule shall show the methods to be used to comply with this requirement.

Delete  subsection 403.05 and replace with the following:

403.05  The accepted quantities of hot bituminous pavement will be paid for in accordance with subsection 401.22, at the contract unit price per metric ton (ton) for the bituminous mixture.

Payment will be made under:

Pay Item 											Pay Unit

Hot Bituminous Pavement (Grading __)(__)(PG ____)		Metric Ton (Ton)

Hot Bituminous Pavement (Grading __)(__)				Metric Ton (Ton)

Hot Bituminous Pavement (Patching)(Asphalt)				Metric Ton (Ton)

Aggregate, asphalt recycling agent, additives, hydrated lime, and all other work necessary to complete each hot bituminous pavement item will not be paid for separately, but shall be included in the unit price bid.  When the pay item includes the PG binder grade, the asphalt cement will not be measured and paid for separately, but shall be included in the work.  When the pay item does not include the PG binder grade, asphalt cement will be measured and paid for in accordance with Section 411.  Asphalt cement used in Hot Bituminous Pavement (Patching) will not be measured and paid for separately, but shall be included in the work.

Excavation, preparation, and tack coat of areas to be patched will not be measured and paid for separately, but shall be included in the work.

Work Sheet, Sheet 4 of 4

January 16, 2004

-4-

REVISION OF SECTION 403

HOT BITUMINOUS PAVEMENT

*********************************************************************************

INSTRUCTIONS TO DESIGNERS (delete instructions and symbols from final draft):

@	Delete from Table 403-1 those pavement gradings and properties not applicable to this project.

x	For Gradings S, SG, and SX insert the designation which is a part of the pay item in the parentheses.  Use additional columns for gradings S, SG, and SX which require separate design mixes for different lab compaction requirements.  Separate pay items with different designations for different lab compaction requirements are to be used.

#	Delete this note when the standard special provision Revision of Section 401 - Reclaimed Asphalt Pavement is included in the project.

&	Add this when excavation and patching in the roadway are required.  Fill in the blank with the Grading used to designate the gradation requirements for patching.

% This requirement is to be included where hydrated lime is needed to prevent stripping, as determined by the District Materials Engineer.

☻Complete this sentence with either "at the location specified in Method A of CP 41" or "at the location specified in either Method B or C of CP 41", as determined by the Region Construction and Materials personnel.  Or, if preferred by the region, delete the sentence altogether.

+	The first three sentences are to be used only on projects where the need for a liquid anti-stripping additive is indicated by engineering considerations.

y	This requirement is to be added when reflective cracking is a concern, such as asphalt overlays of concrete pavement.  Use when directed by the Region.

- See Appendix A of Pavement Design Manual