###### March 11, 2004

REVISION OF SECTIONS 105, 106, AND 412

QUALITY OF PORTLAND CEMENT CONCRETE PAVEMENT (COMPRESSIVE STRENGTH CRITERIA)

##### NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction.  It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions for its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions issued by Project Development Branch unless such use is first approved by the Specification Unit of the Project Development Branch.  The instructions for use on CDOT construction projects appear below.

Other agencies which use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use this standard special provision on appropriate projects with portland cement concrete pavement where the Region has determined that acceptance will be based on compressive strength criteria.

Sections 105, 106 and 412 of the Standard Specifications are hereby revised for this project as follows:

Subsection 105.03 shall include the following:

Conformity to the Contract of all Portland Cement Concrete Pavement, Item 412, will be determined in accordance with the following:

When the Engineer finds that the materials furnished, the work performed, or the finished product does not conform with the Contract, or the Pay Factor (PF) for an element's process is less than 0.75 but that reasonably acceptable work has been produced, the Engineer will determine the extent of the work that will be accepted and remain in place.  The Engineer will use a Contract Modification Order to document the justification for allowing the work to remain in place and the price adjustment that will be applied.

When the Engineer finds the materials furnished, work performed, or the finished product is not in conformity with the Contract, or the PF for an element's process is less than 0.75 and has resulted in an inferior or unsatisfactory product, the work or material shall be removed and replaced or otherwise corrected by and at the expense of the Contractor.  When the PF for any process is 0.75 or greater, the finished quantity of work represented by the process will be accepted at the calculated pay factor.

Materials will be sampled and tested by the Department in accordance with Section 106 and with procedures contained in the Department's Field Materials Manual.  The approximate quantity represented by each sample will be as set forth in Section 106, Table 106-3.  Additional samples may be selected and tested at the Engineer's discretion.

(a)	Incentive/Disincentive Payments (I/DP) will be made based on a statistical analysis that yields Pay Factors (PF) and Quality Levels (QL).  The PF and QL will be made based on test results for the three elements of compressive strength, sand equivalent, and pavement thickness.  Incentive/ Disincentive payment will not be made for thickness of concrete pavement furnished by the Contractor and placed by others.

The QL will be calculated for the elements of compressive strength, sand equivalent and pavement thickness on a process basis.  A separate process will be established for an element when a change in the process affects that element.  A process will consist of the test results from a series of random samples.  Test results determined to have sampling or testing errors will not be used.  All materials produced will be assigned to a process.  A change in process is defined as a change that affects the element involved.  Changes in mix design, material source, design pavement thickness, or the method being utilized to place the pavement are considered changes in process.  The following is provided to clarify changes in processes for each element:

1.	Construction of mainline pavement, including the shoulders if placed with the mainline, is a single process, providing there are no changes in process as described above.

2.	Construction of ramps, acceleration and deceleration lanes, shoulders placed separately and areas requiring hand work are considered separate processes.

3.	A change in the mix design is a process change for the compressive strength element or the flexural strength element, but is not a process change for the pavement thickness element.

(b)	When it is necessary to represent material by one or two tests, each individual test shall have a PF computed in accordance with the following:

If the value of the test is at or above the lower tolerance limit, then PF = 1.000.   If the value of the test is below the lower tolerance limit, then:

PF = 1.00 – [ 0.25(TL -T0)/V ]

where:	PF = pay factor.

V=	V factor from Table 105-6.

T0 = the individual test value.

TL=	 lower tolerance limit.

(c)	The following procedures will be used to compute Incentive/Disincentive Payments (I/DP), quality levels (QL), and pay factors (PF) for processes represented by three or more tests:

1.	Quality Level (QL) will be calculated according to CP-71.

2.	Compute the PF for the process.  When the process has been completed, the number of tests (Pn) it includes shall determine the formula to be used to compute the final pay factor in accordance with the following:

A.	For compressive strength and pavement thickness:

When 3 ≤ Pn ≤ 5

If QL ≥ 85, then PF = 1.00 + (QL - 85)0.001333

If QL < 85, then PF = 1.00 + (QL - 85)0.005208

When 6 ≤ Pn ≤ 9

If QL ≥ 90, then PF = 1.00 + (QL - 90)0.002000

If QL < 90, then PF = 1.00 + (QL - 90)0.005682

When 10 ≤ Pn ≤ 25

If QL ≥ 93, then PF = 1.00 + (QL - 93)0.002857

If QL < 93, then PF = 1.00 + (QL - 93)0.006098

When Pn ≥ 26

If QL ≥ 95, then PF = 1.00 + (QL - 95)0.004000

If QL < 95, then PF = 1.00 + (QL - 95)0.006757

B.	For sand equivalent:

When 3 ≤ Pn ≤ 5

If QL ≥ 85, then PF = 1.00 + (QL - 85)0.000667

If QL < 85, then PF = 1.00 + (QL - 85)0.005208

When 6 ≤ Pn ≤ 9

If QL ≥ 90, then PF = 1.00 + (QL - 90)0.001000

If QL < 90, then PF = 1.00 + (QL - 90)0.005682

When 10 ≤ Pn ≤ 25

If QL ≥93, then PF = 1.00 + (QL - 93)0.001429

If QL < 93, then PF = 1.00 + (QL - 93)0.006098

When Pn ≥ 26

If QL ≥ 95, then PF = 1.00 + (QL - 95)0.002000

If QL < 95, then PF = 1.00 + (QL - 95)0.006757

3.	Compute the I/DP for the process:

I/DP = (PF-1)(QR)(UP)

where:	QR = Quantity Represented by the process.

UP = Unit Price bid for the Item.

The total I/DP for an element shall be computed by accumulating the individual I/DP for each process of that element.

(d)	As acceptance test results become available, they will be used to calculate accumulated QL and  Incentive/Disincentive Payments (I/DP) for each element and for the item.  The Contractor’s test results and the accumulated calculations shall be made available to the Engineer upon request.  The Engineer’s test results and the calculations will be made available to the Contractor as early as reasonably practical. Numbers from the calculations shall be carried to significant figures and rounded according to AASHTO Standard Recommended Practice R-11, Rounding Method.

I/DP will be made to the Contractor in accordance with subsection 412.24(a).  During production, interim I/DP will be computed for information only.  The Pn will change as production continues and test results accumulate.  The Pn at the time an I/DP is computed shall determine the formula to be used.  After all portland cement concrete pavements have been placed according to the contract, the final I/DP will be computed.

(e)	The Contractor will not have the option of accepting a price reduction or disincentive in lieu of producing specification material.  Continued production of non-specification material will not be permitted.  Material which is obviously defective may be isolated and rejected without regard to sampling sequence or location within a process.

Table 105-6

## "V" FACTORS AND INCENTIVE PAYMENTS

| Element | V factor | Maximum Incentive Payment | Lower Tolerance Limit, TL |
| --- | --- | --- | --- |
| Compressive Strength | 2760 kPa (400 psi) | 2.00% | 28 day strength, Table 601-1 |
| Pavement Thickness | 10 mm (0.4 inch) | 2.00% | Plan Thickness –10 mm (-0.4”) |
| Sand Equivalent | 4% | 1.00% | 80% |

Subsection 106.03 shall include the following:

All Portland Cement Concrete Pavement, Item 412, shall be tested in accordance with the following process control and acceptance testing procedures:

(a)	Process Control Testing.  The Contractor shall be responsible for process control testing of all elements listed in Table 106-3.  Process control testing shall be performed at the expense of the Contractor. The Contractor shall develop a quality control plan (QCP) in accordance with the following:

1.	Quality Control Plan.  For each element listed in Tables 106-3, the QCP must provide adequate details to ensure that the Contractor will perform process control.  The Contractor shall submit the QCP to the Engineer at the preconstruction conference.  The Contractor shall not start any work on the project until the Engineer has approved the QCP in writing.

A.	Frequency of Tests or Measurements.  The QCP shall indicate a random sampling frequency, which shall not be less than that shown in Table 106-3.  The process control tests shall be independent of acceptance tests.

B.	Test Result Chart.  Each process control test result, the appropriate area, volume and the tolerance limits shall be plotted.  The chart shall be posted daily at a location convenient for viewing by the Engineer.

C.	Quality Level Chart.  The QL for each element in Table 106-3 shall be plotted.  The QL will be calculated in accordance with the procedure in CP 71 for Determining Quality Level.  The QL will be calculated on tests 1 through 3, then tests 1 through 4, then tests 1 through 5, then thereafter the last five consecutive test results.  The area of material represented by the last test result shall correspond to the QL.

2.	Point of Sampling.  The material for process control testing shall be sampled by the Contractor using approved procedures.  Acceptable procedures are Colorado Procedures, AASHTO and ASTM.  The order of precedence is Colorado Procedures, AASHTO procedures and then ASTM procedures.  The location where material samples will be taken shall be indicated in the QCP.

3.	Testing Standards.  The QCP shall indicate which testing standards will be followed.  Acceptable standards are Colorado Procedures, AASHTO and ASTM.  The order of precedence is Colorado Procedures, AASHTO procedures and then ASTM procedures.

The compressive strength test for process control will be the average strength of two test cylinders cast in plastic molds from a single sample of concrete, cured under standard laboratory conditions, and tested three to seven days after molding.  The trial mix proposed and conducted by the Contractor for mix design approval shall include compressive strength data including the curing time for compressive strength process control tests. CDOT may participate in the process control testing for compressive strength at a frequency determined by the Engineer.

4.	Testing Supervisor Qualifications. The person in charge of and responsible for the process control testing shall be identified in the QCP.  This person shall be present on the project and possess one or more of the following qualifications:

A.	Registration as a Professional Engineer in the State of Colorado.

B.	Registration as an Engineer in Training in the State of Colorado with two years of paving experience.

C.	A Bachelor of Science in Civil Engineering or Civil Engineering Technology with three years of paving experience.

D.	National Institute for Certification in Engineering (NICET) certification at level III or higher in the subfields of Transportation Engineering Technology, Highway Materials or Construction Materials Testing Engineering Technology, Concrete and four years of paving experience.

5.	Technician Qualifications.  Technicians performing tests, if other than the person in responsible charge, shall meet the requirements of Colorado Procedure 10.

6.	Testing Equipment.  All of the testing equipment used to conduct process control testing shall conform to the standards specified in the test procedures and be in good working order.

7.	Reporting and Record Keeping.  The Contractor shall report the results of the tests to the Engineer in writing at least once per day.  The Contractor shall make provisions such that the Engineer can inspect quality control work in progress, including sampling, testing, plants, documentation and the Contractor's testing facilities at any time.

(b)	Acceptance Testing.   Acceptance testing frequencies shall be in accordance with Table 106-3.  Acceptance tests will be conducted by and at the expense of the Department.  Acceptance sampling and testing procedures will be in accordance with the Department's Field Materials Manual with the following exceptions and inclusions:

A split sample from an acceptance test shall not be used for a process quality control test.  The Engineer shall designate the location where samples are to be taken.  Samples shall be taken by the Contractor.  The Engineer will be present during the sampling and take possession of all acceptance samples. Samples transported in different containers will be combined and mixed before molding specimens.  All materials are subject to inspection and testing at all times.

Pavement thickness acceptance will be determined by cores.

The compressive strength test for acceptance will be the average compressive strength of three test cylinders cast in plastic molds from a single sample of concrete and cured under standard laboratory conditions prior to testing.  If the compressive strength of any one specimen differs from the average by more than 10%, that specimen will be deleted and the average strength will be determined using the remaining two specimens.  Each set of three cylinders will be tested at 28 days after molding.

(c)	Check Testing.  The Contractor and the Engineer shall conduct a check testing program (CTP) prior to the placement of any concrete pavement.  The check testing program will include a conference directed by the Region Materials Engineer of the Contractor’s testers and the Department’s testers concerning methods, procedures and equipment for compressive strength testing.  Check testing shall be completed before any portland cement concrete pavement is placed.  A set of three cylinders will be molded by both the Contractor and the Department’s project testers from a split sample.  The specimens will be sampled, molded and cured for seven days and tested for compressive strength according to the procedures of Section 106.  The Department’s Independent Assurance Tester will also mold, cure and test a set of three cylinders, but the Independent Assurance Test results will not be entered in the check testing analysis.  If the results of the check tests do not meet the following criteria, then the check testing will be repeated until the following criteria are met:

1.	The average of the Contractor’s test results and the average of the Department’s test results shall be within 10% of the average of all test results.

- Each specimen test result shall be within 15% of the average of all test results.

A check test must also be conducted on the sand equivalent test.  The average of the absolute differences between the process control and the acceptance testing personnel will be compared to the acceptable limits shown in Table 13-1 of CP-13.  The CTP will be continued until the acceptance and process control test results are within the permissible ranges shown in Table 13-1 of CP-13.

During production, split samples of randomly selected acceptance tests will be compared to the permissible ranges shown in Table 13-1 of CP-13.  The minimum frequency will be as shown in Table 106-3.

If production has been suspended and then resumed, the Engineer may order a CTP between process control and acceptance testing persons to assure the test results are within the permissible ranges shown in Table 106-4.  Check test results shall not be included in process control testing.  The Region Materials Engineer shall be called upon to resolve differences if a CTP shows unresolved differences beyond the ranges shown in Table 13-1 of CP-13.

- Testing Schedule.  All samples used to determine I/DP by quality level formulas in accordance with Section 105, will be selected by a stratified random process.

# TABLE 106-3

# TESTING SCHEDULE - ITEM 412  PORTLAND CEMENT CONCRETE PAVEMENT

| Element | Minimum Testing Frequency Contractor's Process Control | Minimum Testing Frequency CDOT Acceptance Testing |
| --- | --- | --- |
| Aggregate Gradation and Fractured Faces | 1/10 000 m2 (1/10,000 sq. yds.) or one/day if less than 10 000 m2 (10,000 sq. yds.) are placed in a day. | None |
| Slump | First three loads each day, then as needed for control. | Witness by the Engineer. |
| Compressive Strength, Air Content, (Yield and Sand Equivalent | 1/2500 m2 (1/2500 sq. yds.) or one/day if less than 2500 m2 (2500 sq. yds.) are placed in a day. | Minimum of 1/day. If the project total < 50 000 m2 (50,000 sq. yds.), then a minimum of ten tests. If the project total ≥50 000 m2 (50,000 sq. yds.), then 1/5000 m2 (1/5,000 sq. yds.). |
| Pavement Thickness | In accordance with subsection 412.21. | Minimum of 1/day. If the project total < 50 000 m2 (50,000 sq. yds.), then a minimum of ten tests. If the project total ≥ 50 000 m2 (50,000 sq. yds.), then 1/5000 m2 (1/5000 sq. yds.). |
| Pull Test Joints | Minimum of six transverse and six longitudinal joint locations in each 760 m (2500 linear feet). | Witness by the Engineer. |
| Load Transfer Dowel Bar Placement | Minimum of six transverse joint locations in each 760 m (2500 linear feet). | Witness by the Engineer. |
| Tining Depth | 1 per 160 m (528 linear feet) in each lane and shoulder wider than 2.4 m (8 feet). | Witness by the Engineer. |

(Yield is for information only.

In subsection 412.21, delete the fifth through tenth paragraphs and replace with the following:

The lower tolerance limit (TL) for pavement thickness shall be Plan Thickness (PT) minus 10 mm (0.4 inches).  This TL shall be used in the formulas in Section 105 for Incentive/Disincentive Payments (I/DP), Quality Levels (QL) and Pay Factor (PF) determinations. Any pavement thickness test value that exceeds the PT by more than 25 mm (1.0 inch) shall be assigned a value of PT + 25 mm (1.0 inch) for the purpose of calculating the QL, PF and I/DP.

Coring frequency shall be in accordance with subsection 106.03.  Core locations shall be determined by a random procedure so that each area has a randomly selected coring location.  One core will be taken at each location.

Where the new portland cement concrete pavement overlays an existing roadway, cores for measuring pavement thickness shall be determined by a stratified random procedure in the longitudinal direction and by the point of minimum required thickness in the lateral direction as shown in the plans.  If existing field conditions show a condition where the point of minimum thickness in the lateral direction as shown in the plans is not appropriate, the Contractor shall identify the location and extent of the area to the Engineer at least 24 hours before paving.  The Engineer may exclude this area from pavement thickness measurements for incentive/disincentive payments.

Pavement thickness tests will be evaluated in accordance with subsection 105.03.

Additional cores will be taken at the direction of the Engineer as follows:

(1)	One additional core at the location of each process control (PC) test that is less than TL but greater than PT minus 25 mm (1.0 inch).  If the length of the additional core is greater than TL, no additional actions will be taken and the original randomly selected acceptance test core will be used to compute I/DP for the process that includes this material.

(2)	If the additional core or any randomly selected core is less than TL but greater than PT minus 25 mm (1.0 inch), the area represented by this core shall become a separate process and this core will not be used to compute an I/DP.  Four additional randomly selected cores will be taken within the area represented by this core.  The four additional cores will be used to compute an I/DP in accordance with Section 105.  Cores taken at locations not randomly determined, such as process control cores will not be used to compute I/DP.

(3)	When the measurement of any core is less than PT (Plan Thickness) minus 25 mm (1.0 inch), whether randomly located or not, the area represented by this core shall become a separate process and this core will not be used to compute an I/DP.  The actual thickness of the pavement in this area will be determined by taking exploratory cores.  Cores shall be taken at intervals of 4.6 m (15 feet) or less, parallel to the centerline in each direction from the affected location until two consecutive cores are found in each direction which are not less than PT minus 25 mm (1.0 inch).

Pavement areas found to be less than PT minus 25 mm (1.0 inch) shall be removed and replaced at the Contractor's expense.  Exploratory cores taken at the Contractor's expense will be used to determine the extent of deficient pavement for pavement removal.

When the removal and replacement have been completed, four additional randomly selected cores will be taken within the area represented by this core.  The four additional cores will be used to compute an I/DP in accordance with subsection 105.03.  Exploratory cores will not be used to compute I/DP.

The Contractor shall repair all core holes by filling them with an approved non-shrink high strength grout.

Subsection 412.24(a) shall include the following:

Incentive/Disincentive Payments (I/DP) will not be made on interim estimates.  I/DP will be made when the concrete pavement or a major phase of the concrete pavement has been completed and all the data for computing the I/DP is available.

Delete subsection 412.24(b) and replace with the following:

(b)	Where the pavement thickness is more than Plan Thickness (PT) minus 25 mm (1.0 inch), I/DP for the element of pavement thickness will be applied to the contract unit price in accordance with subsections 105.03 and 412.21.  I/DP for other elements will be applied to the contract unit in accordance with Sections 105 and 412.

Adjustments in payment because of deviations in air content will be in accordance with subsection 601.17 using $131/m3 ($100.00 per cu. yd.) for the unit bid price.