### March 11, 2004

# REVISION OF SECTION 208

STABILIZED CONSTRUCTION ENTRANCE

## NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction.  It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions regarding its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by the Standards and Specifications Unit of the Project Development Branch.  The instructions for use on CDOT construction projects appear below.

Other agencies that use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use this standard special provision on projects having stabilized construction entrances as part of erosion control measures.

March 11, 2004

REVISION OF SECTION 208

STABILIZED CONSTRUCTION ENTRANCE

Section 208 of the Standard Special Provisions is hereby revised for this project as follows:

Subsection 208.01 shall include the following:

This work consists of constructing a stabilized construction entrance, as shown in the plans, or as directed by the Engineer.

Subsection 208.02 shall include the following:

- Stabilized Construction Entrance.  Construction of approved stabilized construction entrances shall be completed before any excavation or work is started between such entrances, as shown on the plans.

Unless otherwise directed by the Engineer, aggregate for the construction entrance shall be coarse material that meets the following gradation requirements:

Sieve size			Mass Percent Passing Square Mesh Sieves

3 inch				100

2 inch				95-100

¾ inch				0-15

Geotextile shall conform to the requirements of subsection 420.06.

Subsection 208.05 shall include the following:

- Stabilized construction entrance.  Stabilized construction entrances shall be constructed to the minmum dimensions shown on the plans, unless otherwise directed by the Engineer.

The Contractor shall be responsible for maintaining the stabilized construction entrance during the entire time that it is in use in the project. The stabilized construction entrance shall be removed at the completion of this project unless otherwise directed by the Engineer.

Subsection 208.07 shall include the following:

Stabilized construction entrance will be measured by the actual number that are constructed and accepted.

Subsection 208.08 shall include the following:

Payment will be made under:

### Pay Item					Pay Unit

Stabilized Construction Entrance		Each

Payment will be full compensation for all work, materials and equipment required to construct, maintain, and remove the entrance upon completion of the work.

Aggregate and geotextile will not be measured and paid for separately, but shall be included in the work.