### May 26, 2005

REVISION OF SECTIONS 702

# SUPERPAVE PG BINDERS

#### NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction.  It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions regarding its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by the Standards and Specifications Unit of the Project Development Branch.  The instructions for use on CDOT construction projects appear below.

Other agencies that use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use this standard special provision on projects with hot bituminous pavement with Superpave performance graded binders.

May 26, 2005

-1-

REVISION OF SECTION 702

SUPERPAVE PG BINDERS

Section 702 of the standard specifications is hereby revised for this project as follows:

Subsection 702.01(a) shall include the following:

Asphalt cement shall not be acid modified or alkaline modified.

Asphalt cement shall not contain any used oils that have not been re-refined for resale.  In addition, no modifiers shall be added that do not comply with environmental rules and regulations including 40 CFR Part 261.6(a) (3) (v), and part 266/Subpart C.  Modifiers shall not be carcinogenic.

In subsection 702.01(b) delete Table 702-2 and replace with the following:

# Table 702-2

# SuperPave Performance Graded Binders

| Property | Requirement for PG Binder | AASHTO Test No. |
| --- | --- | --- |
|  | 58-28 | 58-34 | 64-22 | 64-28 | 76-28 |  |
| Original Binder Properties |  |  |  |  |  |  |
| Flash Point Temp., °C, minimum | 230 | 230 | 230 | 230 | 230 | T 48 |
| Viscosity at 135 °C, Pa●s, maximum | 3 | 3 | 3 | 3 | 3 | TP 48 |
| Dynamic Shear, Temp. °C, where G*/Sin δ @ 10 rad/s ≥ 1.00 kPa | 58 | 58 | 64 | 64 | 76 | TP 5 |
| Ductility, 4 °C (5 cm/min.), cm minimum | - | - | - | 50 | - | T 51 |
| Toughness, joules (inch-lbs) | - | - | - | 12.4 (110) | - | *CP L-2210 |
| Tenacity, joules (inch-lbs) | - | - | - | 8.5 (75) | - | *CP L-2210 |
| Acid or Alkali Modification (pass-fail) |  |  |  |  |  | *CP L-2214 |
| RTFO Residue Properties |  |  |  |  |  | CP-L 2215 |
| Mass Loss, percent maximum | 1.00 | 1.00 | 1.00 | 1.00 | 1.00 | CP-L 2215 |
| Dynamic Shear, Temp. °C, where G*/Sin δ @ 10 rad/s ≥ 2.20 kPa | 58 | 58 | 64 | 64 | 76 | TP 5 |
| Elastic Recovery, 25 °C, percent min. | - | - | - | - | 50 | *CP L-2211 Method A |
| Ductility, 4 °C (5 cm/min.), cm minimum | - | - | - | 20 | - | T 51 |
| PAV Residue Properties, Aging Temperature 100 °C |  |  |  |  |  | PP 1 |
| Dynamic Shear, Temp. °C, where G*●Sin δ @ 10 rad/s ≤ 5000 kPa | 19 | 16 | 25 | 22 | 28 | TP 5 |
| Creep Stiffness, @ 60 s, Test Temperature in °C | -18 | -24 | -12 | -18 | -18 |  |
| S, maximum, MPa | 300 | 300 | 300 | 300 | 300 | TP 1 |
| m-value, minimum | 0.300 | 0.300 | 0.300 | 0.300 | 0.300 | TP 1 |
| **Direct Tension, Temperature in °C, @ 1 mm/min., where failure strain ≥ 1.0 % | -18 | -24 | -12 | -18 | -18 | TP 3 |
| *Colorado Procedure **Direct tension measurements are required when needed to show conformance to AASHTO MP 1. |

May 26, 2005

-2-

REVISION OF SECTION 702

SUPERPAVE PG BINDERS

In subsection 702.01 (b) delete the last four paragraphs and replace with the following:

The supplier of the PG binder shall be certified in accordance with CP 11

Samples of the PG binder for acceptance shall be sampled on the project as stated in the Schedule of the Field Materials Manual.

The Department will test for acid modification and alkaline modification during the binder certification process.  Thereafter, the Department will randomly test for acid modification and alkaline modification.