###### October 13, 2005

# REVISION OF SECTION 702

ASPHALT EMULSIONS

## NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction.  It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions regarding its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by the Standards and Specifications Unit of the Project Development Branch.  The instructions for use on CDOT construction projects appear below.

Other agencies that use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use this standard special provision on projects having pay Items from Sections 405, 406, 407, 409 or 411.

## August 30,

October 13, 2005

1

REVISION OF SECTION 702

ASPHALT EMULSIONS

Section 702 of the Standard Specifications is hereby revised for this project as follows:

In subsection 702.03 delete the second sentence in the first paragraph and replace with the following:

Emulsified asphalt and aggregate used for seal coats shall be sampled and will be tested for information only according to CP-L 2213, Chip Seal Compatibility.

In subsection 702.03 delete  (a), including Tables 702-4 and 702-5, and replace with the following:

Polymerized emulsions for seal coat shall conform to the requirements listed in Table 702-4.   Emulsion for seal coat shall be an emulsified blend of polymerized asphalt, water, and emulsifiers. The asphalt cement shall be polymerized prior to emulsification and shall contain a minimum of 3.0 percent polymer by weight of asphalt cement.  The emulsion standing undisturbed for a minimum of 24 hours shall show no white, milky separation but shall be smooth and homogeneous throughout.  The emulsion shall be pumpable and suitable for application through a distributor.

October 13, 2005

2

REVISION OF SECTION 702

ASPHALT EMULSIONS

Table 702-4

| Property | CRS-2P | CMS-2P | HFRS-2P | HFMS-2P | AASHTO Test No. |
| --- | --- | --- | --- | --- | --- |
| Tests on Emulsion: |  |  |  |  |  |
| Viscosity, at 50ºC, Sabolt- Furol, s | min | 50 | 50 | 50 | 50 | T 59 |
|  | max | 450 | 450 | 450 | 450 |  |
| Storage stability, 24 hr, % max | 1.0 | 1.0 | 1.0 | 1.0 | T 59 |
| Particle charge test | Positive | Positive |  |  | T 59 |
| Sieve test, % max | 0.10 | 0.10 | 0.10 | 0.10 | T 59 |
| Demulsibility, % min | 40 |  | 40 |  | T 59 |
| Oil Distillate by volume, % max or range | 3.0 | 3.0 | 3.0 | 3.0 | T-59 |
| Residue by distillation/ evaporation2, % min | 652 | 652 | 652 | 652 | T 59/ CP-L 22121 3 |
| Tests on residue: |  |  |  |  |  |
| Penetration, 25ºC, 100g, 5s, min | 70 | 70 | 70 | 70 | T 49 |
| Penetration, 25ºC, 100g, 5s, max | 150 | 150 | 150 | 150 |  |
| Ductility, 25ºC, 5 cm/min, cm, min |  |  | 75 | 75 | T 51 |
| Solubility, in trichloroethylene% min | 97.5 | 97.5 | 97.5 | 97.5 | T 44 |
| Elastic Recovery, 25ºC min |  |  | 58 | 58 | CP-L 22113 |
| Float Test, 60ºC, s min |  |  | 1200 | 1200 | T 50 |
| Toughness, in-lbs, min | 70 | 70 |  |  | CP-L 22103 |
| Tenacity, in-lbs, min | 45 | 45 |  |  | CP-L 22103 |
| 1 CP-L 2212 is a rapid evaporation test for determining percent residue of an emulsion and providing material for tests on residue. CP-L 2212 is for acceptance only. If the percent residue or any test on the residue fails to meet specifications, the tests will be repeated using the distillation test in accordance with AASHTO T-59 to determine acceptability. 2 For polymerized emulsions the distillation and evaporation tests will in be in accordance with AASHTO T-59 or CP-L 2212 respectively with modifications to include 205 ± 5ºC (400 ± 10ºF) maximum temperature to be held for 15 minutes. 3 Colorado Procedure - Laboratory |

October 13, 2005

3

REVISION OF SECTION 702

ASPHALT EMULSIONS

In subsection 702.03 delete the last sentence of the note at the bottom of table 702-8 and replace with the following:

Emulsified Asphalt (HFMS-2sP) with a residual penetration greater than 300 mm shall meet all properties listed in Table 702-8, except that Elastic Recovery shall be reported for information only.

Subsection 702.04 shall include the following:

For hot-in-place recycling ARA 1P is an acceptable alternative to ARA.  ARA-1P shall meet the requirements below:

Emulsified Polymer Modified Asphalt Rejuvenating Agent (ARA-1P) for use in hot-in-place recycling of bituminous pavements shall be modified with a minimum of 1.5% styrene-butadiene solution polymer and shall not contain any used oils that have not been re-refined or reprocessed.  In addition, no modifiers shall be added that do not comply with environmental rules and regulations including 40 CFR Part 261.6(a)(3)(v), and part 266/Subpart C.  Modifiers shall not be carcinogenic.  The finished product shall conform to the physical requirements listed in Table 702-10A below.

# Table 702-10A

| Test on Emulsion | Test Method | Min | Max |
| --- | --- | --- | --- |
| Viscosity, Saybolt-Furol @ 77ºF, s | ASTM D 244 | 15 | 100 |
| Residue @ 350ºF, % | ASTM D244 Mod | 60 |  |
| Sieve Test, % | ASTM D244 |  | 0.10 |
| Oil distillate, % | ASTM D244 |  | 2.0 |
| Test on Residue | Residue from D244 Mod |  |  |
| Penetration @ 39.2ºF, 100g, 5s | ASTM D-5 Modified | 150 | 250 |
| Asphaltenes, % | ASTM D4124 |  | 15 |