October 13, 2005

REVISION OF SECTION 401

LONGITUDINAL JOINTS

NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction  It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions for its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by CDOT’s Standards and Specifications Unit.  The instructions for use on CDOT construction projects appear below.

Other agencies which use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use this standard special provision on all projects having any grade of hot mix asphalt.

October 13, 2005

REVISION OF SECTION 401

LONGITUDINAL JOINTS

Section 401 of the Standard Specifications is hereby revised for this project as follows:

In subsection 401.17, delete the fifth paragraph and replace with the following:

The Contractor shall obtain one 6-inch diameter core at a random location within each longitudinal joint sampling section for determination of the joint density.  The Contractor shall mark and drill the cores at the location directed by the Engineer and in the presence of the Engineer.  The Engineer will take possession of the cores for testing.  The Contractor may take additional cores at the expense of the Contractor.  Coring locations shall be centered on the visible line where the joint between the two adjacent lifts abut at the surface. The center of all joint cores shall be within ± 1 inch of this visible joint line. Core holes shall be repaired by the Contractor using materials and methods approved by the Engineer. QC and QA joint coring shall be completed within five calendar days of joint construction.

Longitudinal joint coring applies to all pavement lifts. When constructing joints in an echelon paving process, the joints shall be clearly marked to ensure consistent coring location. In small areas, such as intersections, where the Engineer prescribes paving and phasing methods, the Engineer may temporarily waive the requirement for joint density testing.