# MEMORANDUM

# DEPARTMENT OF TRANSPORTATION

Project Development Branch

# 4201 East Arkansas Avenue

Denver, Colorado 80222

(303)757-9040

FAX (303)757-9868

# DATE:	March 18, 2005

# TO:	All Holders of Standard Special Provisions

# FROM:	Mithilesh Kumar, Project Development Branch

# SUBJECT:	Revision of Sections 105 and 106, Quality of Hot Bituminous Pavement

# Attached is a revised standard special provision, Revision of Sections 105 and 106, Quality of Hot Bituminous Pavement, 11 pages, dated March 18, 2005.  Use this standard special provision on projects having 5000 or more tons of hot bituminous pavement when acceptance is based on gradation, asphalt content, and in-place density, beginning with projects advertised on or after April 14, 2005.  Earlier use is permissible.

# This revised standard special provision replaces one of the same title dated January 16, 2004.  This revision defines the minimum quality level of air voids, AC content, and VMA for mixture verification.  This is being done to minimize the risk of using a mix that has low AC contents and low VMA, but which still could potentially meet the mix verification under the current specification.

# Please replace the superseded version of this standard special provision with this revised version.  A new Index of Standard Special Provisions dated March 18, 2005 is attached.

# mrs/mk

# Attachments

# Distribution: Per distribution list