December 8, 2005

REVISION OF SECTION 703

AGGREGATE FOR STONE MATRIX ASPHALT

NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction  It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions for its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by CDOT’s Standards and Specifications Unit.  The instructions for use on CDOT construction projects appear below.

Other agencies which use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use on projects having stone matrix asphalt.

December 8, 2005

REVISION OF SECTION 703

AGGREGATE FOR STONE MATRIX ASPHALT

Section 703 of the Standard Specifications is hereby revised for this project as follows:

In subsection 703.04, delete Table 703-5 and replace with the following:

Table 703-5

Master Range Table for Stone Matrix Asphalt

| Sieve Size | Percent by Weight Passing Square Mesh Sieves |
| --- | --- |
|  | 4.75 mm (#4) nominal | 9.5 mm (3/8”) nominal | 12.5 mm (1/2”) nominal | 19.0 mm (3/4”) nominal |
| 25 mm (1”) |  |  |  | 100 |
| 19.0 mm (3/4”) |  |  | 100 | 90-100 |
| 12.5 mm (1/2”) | 100 | 100 | 90-100 | 50-88 |
| 9.5 mm (3/8”) | 100 | 90-100 | 50-80 | 25-60 |
| 4.75 mm (#4) | 90-100 | 26-60 | 20-35 | 20-28 |
| 2.36 mm (#8) | 28-65 | 20-28 | 16-24 | 16-24 |
| 1.18mm (#16) | 22-36 |  |  |  |
| 600 µm (#30) | 18-28 | 12-18 | 12-18 | 12-18 |
| 300 µm (#50) | 15-22 | 10-15 |  |  |
| 150 µm (#100) |  |  |  |  |
| 75 µm (#200) | 12-15 | 8-12 | 8-11 | 8-11 |