412pccptw

04-07-06

REVISION OF SECTION 412

## PORTLAND CEMENT CONCRETE PAVEMENT

## THIN WHITETOPPING

Section 412 of the Standard Specification is hereby revised for this project as follows:

Subsection 412.03 shall include the following.

Concrete for thin whitetopping shall conform to the requirements for Class P as described in subsections 601.02 and 601.03 with the following exception: Class P for thin whitetopping shall contain a minimum of 55 percent coarse aggregate.  Coarse aggregate shall conform to AASHTO M43, Size 467.  Class E shall be used where FastTrack concrete is required.

Subsection 412.10 shall include the following.

Thin whitetopping shall be placed in accordance with the following additional requirements:

- The Contractor shall receive delivery tickets, monitor and maintain yield to achieve the minimum thickness.  Copy of tickets shall be delivered to the Engineer at the end of each days paving.

- Surface Milling: The milled surface shall be full-width.  Concrete shall not be placed on un-milled surfaces.  If the base is exposed, the Contractor shall submit a plan to correct the exposed base surface and proceed with corrective action upon approval of the plan.  The milled surface shall not be open to traffic.

- Surface Cleaning: The initial cleaning of the milled surface shall be accomplished by brooming the surface using a mechanical broom.  The surface shall be further cleaned by the use of pressure cleaning to ensure that all dust, grit, and foreign material is removed from the surface.  The area shall be protected as necessary to prevent contamination until placement.  When areas are not adequately protected, the Contractor shall perform additional cleaning prior to placement of concrete overlay as directed.

- Moisture Coat: After the surface has been milled, cleaned, and accepted, and prior to the concrete overlay placement, a moisture coat shall be placed on the prepared surface.  The Contractor shall spray a light mist just ahead of the concrete placement in a manner that does not cause ponding.  Concrete overlay shall occur immediately following this moisture coat, while the surface is still wet.

Concrete pavement for thin whitetopping shall be placed to the depth specified in the Contract.  Additional concrete pavement for thin whitetopping shall be placed at locations of grade adjustments and irregularities as approved by the Engineer.

Subsection 412.21 shall include the following:

The thickness of concrete pavement thin whitetopping shall be controlled and determined by the following simultaneous methods:

- The Contractor shall control the paver grade by using a string line pulled from pin to pin in front of the paver at intervals not greater than 50 feet.

- The thickness of the plastic concrete shall be determined by taking stab depth measurements during paving at intervals not greater than 100 feet intervals.  The Contractor shall stab and measure at the lane lines.  When the edge of the concrete being placed falls at a lane line, the measurement shall be offset two feet from that line.  The Contractor shall keep a log (date, before or behind paver, depth, station and offset) of these measurements and provide the Engineer a copy every week, unless otherwise requested.

In subsection 412.23, first paragraph, delete the first sentence and replace it with the following:

The quantities of Concrete Pavement, Concrete Pavement Thin Whitetopping, and Place Concrete Pavement to be paid for under these items will be measured by the square yards completed and accepted.

Subsection 412.23, second paragraph, shall include the following after the second sentence:

Furnish Concrete Pavement Thin Whitetopping will be measured by the cubic yards of additional concrete required at locations of grade adjustments and irregularities.

Subsection 412.24 (a) shall include the following:

Pay Item								Pay Unit

Concrete Pavement Thin Whitetopping (__ Inch)				Square Yard

Furnish Concrete Pavement Thin Whitetopping				Cubic Yard

The price per square yard of Concrete Pavement Thin Whitetopping (__ Inch) shall be full compensation for furnishing and placing all materials, including any dowels, tie bars, joint materials, tining, sawing, finishing and rumble strips.

Concrete Class E for FastTrack will not be measured and paid for separately, but shall be included in the work.