Sample project special: 401703smap

10-19-06

REVISION OF SECTIONS 401 AND 703

STONE MATRIX ASPHALT PAVEMENT

Sections 401 and 703 of the Standard Specifications are hereby revised for this project as follows:

Subsection 401.02 shall include the following:

Recycled Asphalt Pavement (RAP) shall not be used in Stone Matrix Asphalt (SMA) mix.

Subsection 401.09 shall include the following:

Each SMA load shall be completely covered and securely fastened with a full tarp.

Subsection 401.16 shall include the following:

The SMA mixture shall be transported and placed on the roadway without drain-down or flushing.  All flushed areas behind the paver shall be removed immediately upon discovery.  If more than 50 square feet of flushed SMA pavement is ordered removed and replaced in any continuous 500 linear feet of paver width laydown, operations shall be discontinued until the source of the flushing has been found and corrected. The Contractor is responsible for all expenses associated with removal and replacement of all flushed areas.  The Engineer shall designate the depth and area of all flushed areas requiring removal and replacement.

Subsection 401.17 shall include the following:

Rollers shall not be used in a vibratory mode on SMA unless they are first used successfully in the demonstration control strip specified in subsection 403.03.  Pneumatic wheel rollers shall not be used on SMA mix.

The relative compaction for all SMA mixtures will be measured from roadway cores in accordance with CP 44, Method B, unless the SMA mixture is being placed on a structure (bridge deck) in which case the Engineer may specify that nuclear gauge measurements be used.

When cores are used, the Contractor shall provide all labor and equipment for the coring operation and filling the core holes.  When nuclear density gauges are used, the tests will be performed in accordance with CP 81 and CP 82.

In-place density for SMA shall be 93 to 97 percent of the SMA mix maximum specific gravity as measured according to CP 51.

Subsection 401.22 shall include the following:

Acceptance, testing, and pay factors for SMA shall be in accordance with subsections 105.05 and 106.05 as revised for this project for Hot Mix Asphalt.

-2-

REVISION OF SECTIONS 401 AND 703

STONE MATRIX ASPHALT PAVEMENT

Subsection 703.06 shall include the following:

Mineral filler for the Stone Matrix Asphalt pavement shall be limestone dust and shall meet the requirements of this subsection and the following:

Plasticity Index (AASHTO T90)              4% Maximum

The Contractor shall submit hydrometer analysis (AASHTO T88) for the mineral filler used in the SMA mix.

INSTRUCTIONS TO DESIGNERS

The Standard Special Provision, Revision of Section 703, Aggregate for Stone Matrix Asphalt, and the Project Special Worksheet, Revision of Section 403, Stone Matrix Asphalt Pavement, must be used along with this specification.

In addition, the Standard Special Provision for gradation acceptance of HMA must be included with this specification to provide construction and acceptance requirements.  Choose the appropriate specification from the two listed below, based on the quantity of Stone Matrix Asphalt:

Revision of Sections 105 and 106, Conformity to the Contract of Hot Mix Asphalt

Revision of Sections 105 and 106, Conformity to the Contract of Hot Mix Asphalt (Less Than 5000 Tons)