Sample Project Special Provision: 401ts

10-19-06

REVISION OF SECTION 401

Temperature Segregation

Section 401 of the Standard Specifications is hereby revised for this project as follows:

Subsection 401.16 shall include the following:

The Engineer will perform a systematic segregation check in accordance with CP 58 as early in the project as is feasible to determine if temperature segregation problems exist.  Temperature segregation will be of concern on the project if, across the width of the mat, temperatures vary by 25 °F or more.  Densities will not need to be taken in the systematic segregation study.  The Engineer will discuss the temperature findings of the systematic segregation check with the Contractor.

The Engineer may evaluate the HMA for low density due to temperature segregation any time industry best practices, as detailed on Form 1346, are not being followed or the Engineer suspects temperature segregation is occurring.  The Engineer will first meet with the Contractor to discuss the paving practices that are triggering the temperature investigation.  Areas across the mat, excluding the outside 1 foot of both edges of the mat, that are more than 25 °F cooler than other material across the width may be marked for density testing.  Material for temperature comparison will be evaluated in 3-foot intervals behind the paver across the width of the mat.  The material shall be marked and tested in accordance with CP 58.  If four or more areas within a lot of 500 tons have densities of less than 92 percent of the material’s maximum specific gravity, a 5 percent price disincentive will be applied to the 500 ton lot.  The 500 ton count begins when the Engineer starts looking for cold areas, not when the first cold area is detected.  This price disincentive will be in addition to those described in Sections 105 and 106.  Only one area per delivered truck will be counted toward the number of low density areas.  This specification shall only be applied in areas where continuous paving is possible.