November 30, 2006

REVISION OF SECTION 208

SILT BERM

NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction  It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions for its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by CDOT’s Standards and Specifications Unit.  The instructions for use on CDOT construction projects appear below.

Other agencies which use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use on projects having silt berms.

November 30, 2006

REVISION OF SECTION 208

SILT BERM

Section 208 of the Standard Specifications is hereby revised for this project as follows:

Subsection 208.01 shall include the following:

This work includes the installation of a silt berm, to reduce erosion in temporary ditches, permanent ditches, and borrow ditches as shown on the plans.

In subsection 208.02, delete (e) and replace with the following:

- Silt Berm.  Silt berm shall consist of an ultraviolet (UV) stabilized high-density polyethylene, shall be triangular in shape and shall have the following dimensions:

| Width | 6 - 11 inches |
| --- | --- |
| Height | 6 - 10 inches |
| Weight | 0.3 - 1.4 lbs./sq. ft. |
| Percent Open Area | 30 – 50% |

In subsection 208.05, delete (g) and replace with the following:

- Silt Berm.  Prior to installation of silt berms, the Contractor shall prepare the surface of the areas in which the berms are to be installed such that are they free of materials greater than 2 inches in diameter and are suitably smooth for the installation of the silt berms, as approved.

Berms shall be secured with 10 to12 inch x 0.375-inch diameter (minimum) spikes.    A minimum one spike per foot shall be installed on both sides of each berm and in accordance with manufacturer’s recommendations. The Contractor shall install the berm in a manner that will prevent water from going around or under the silt berm. If silt berms are installed in combination with soil retention blanket, then the silt berms shall be installed on top of installed blanket.

Subsection 208.07 shall include the following:

Silt berms will be measured by the actual number of linear feet of berm that is installed and accepted.

Subsection 208.08 shall include the following:

# Pay Item			Pay Unit

Silt Berm			Linear Foot

Spikes will not be measured and paid for separately, but shall be included in the work.

When required, soil retention blankets will be measured and paid for in accordance with Section 216.