April 12, 2007

REVISION OF SECTIONS 601, 606, 608, 609 AND 618

CONCRETE FINISHING

NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction  It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions for its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by CDOT’s Standards and Specifications Unit.  The instructions for use on CDOT construction projects appear below.

Other agencies which use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use on projects having any type of concrete construction

April 12, 2007

REVISION OF SECTIONS 601, 606, 608, 609, AND 618

CONCRETE FINISHING

Sections 601, 606, 608, 609, and 618 of the Standard Specifications are hereby revised for this project as follows:

Subsection 601.12 (a) shall include the following:

Unless otherwise specified, hand finishing methods will be permitted only when performed under the direct supervision of a Craftsman holding the following certificate:  ACI Concrete Flatwork Finisher and Technician (ACICFFT) or other Flatwork Finisher certification program approved by the Department. A minimum of one certified Craftsman is required at each finishing operation.  A minimum of one certified Craftsman is required for each three or fewer finishers (non-certified ACICFFTs) at each operation.

Subsection 601.14(a) shall include the following:

The finishing of hardened concrete surfaces shall not require a certified Concrete Flatwork Finisher as described in subsection 601.12(a).

Subsection 606.04(a), second paragraph, shall include the following:

When hand finishing is allowed, it shall be performed under the supervision of a certified Concrete Flatwork Finisher in conformance with revised subsection 601.12(a).

Subsection 606.04(b), first paragraph, shall include the following:

All required hand finishing shall be performed under the supervision of a certified Concrete Flatwork Finisher in conformance with revised subsection 601.12(a).

Subsection 608.03(d), first paragraph, shall include the following:

All required hand finishing shall be performed under the supervision of a certified Concrete Flatwork Finisher in conformance with revised subsection 601.12(a).

Subsection 609.03 shall include the following:

All required hand finishing shall be performed under the supervision of a certified Concrete Flatwork Finisher in conformance with revised subsection 601.12(a).

Subsection 618.11(f), first paragraph, shall include the following:

All required hand finishing shall be performed under the supervision of a certified Concrete Flatwork Finisher in conformance with revised subsection 601.12(a).