Sample Project Special Provision: 208gb

10-25-07

REVISION OF SECTION 208

Gravel Bag

Section 208 of the Standard Specifications is hereby revised for this project as follows:

Subsection 208.01 shall include the following:

This work consists of the installation of gravel bags at locations  shown on the plans.

Subsection 208.02 shall include the following:

(o) Gravel Bag.  Gravel bags shall consist of aggregate filled fabric with the following dimensions:

Diameter		                     4 to 6 inches

Section Length		1 foot minimum

The sediment control device shall consist of a woven geotextile fabric with the following properties:

| Grab tensile strength | 90 lbs. min. | ASTM D 4632 |
| --- | --- | --- |
| Trapezoid Tear Strength | 25 lbs. min. | ASTM D 4533 |
| Mullen Burst | 300 psi. | ASTM D 3786 |
| Ultraviolet Resistance | 70% | ASTM D 4355 |

Gravel bags shall be capable of remaining in place during a storm event.  Aggregate contained in the gravel bags shall consist of gravel or crushed stone conforming to Table 703-7 for Class C.

Subsection 208.05 shall include the following:

- Gravel Bag. Gravel bags shall be placed on a stable surface, consisting of pavement, grass or aggregate. Gravel bags shall be placed to conform to the surface without gaps.  Discharge water shall not cause erosion.

Subsection 208.07 shall include the following:

Gravel Bags will be measured by the linear foot of bags that are installed and accepted.

Subsection 208.08 shall include the following:

# Pay Item			Pay Unit

Gravel Bag			Linear Foot

Payment will be full compensation for all work, materials and equipment required to complete the item, including surface preparation, maintenance throughout the project, and removal upon completion of work.

Aggregate will not be measured and paid for separately, but shall be included in the work.