# October 25, 2007

REVISION OF SECTION 712

HYDRATED LIME

NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction.  It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions for its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by the Standards and Specifications Unit of the Project Development Branch.  The instructions for use on CDOT construction projects appear below.

Other agencies which use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use this standard special provision on projects having HMA or SMA.

October 25, 2007

REVISION OF SECTION 712

HYDRATED LIME

Section 712 of the Standard Specifications is hereby revised for this project as follows:

Delete subsection 712.03 and replace with the following:

712.03  Hydrated Lime.  The hydrated lime for Hot Mix Asphalt (HMA) and Stone Matrix Asphalt (SMA) shall conform to the requirements of AASHTO M 303, Type I. In addition, the particle size requirements shall conform to AASHTO M 303 when tested in accordance with CP-L 4209 Physical Testing of Quicklime, Hydrated Lime, and Limestone.