January 17, 2008

REVISION OF SECTION 401

TOLERANCES FOR HOT MIX ASPHALT

NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction.  It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions for its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by the Standards and Specifications Unit of Project the Development Branch.  The instructions for use on CDOT construction projects appear below.

Other agencies which use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use this standard special provision on projects with hot mix asphalt when acceptance is based on asphalt content, gradation, and in-place density.

January 17, 2008

REVISION OF SECTION 401

TOLERANCES FOR HOT MIX ASPHALT

Section 401 of the Standard Specifications is hereby revised for this project as follows:

In subsection 401.02(b) delete Table 401-1 and replace with the following:

Table 401-1

Tolerances for Hot Mix Asphalt

| Asphalt Content | ± 0.3% |
| --- | --- |
| Asphalt Recycling Agent | ± 0.2% |
| 1Hot Mix Asphalt – Item 403 |  |
| 2Passing the 9.5 mm (3/8 inch) and larger sieves | ± 6% |
| 2Passing the 4.75 mm (No. 4) and 2.36 mm (No. 8 ) sieves | ± 5% |
| 2Passing the 600 (m (No. 30) sieve | ± 4% |
| 2Passing the 75 (m (No. 200) sieve | ± 2% |
| 1When 100% passing is designated, there shall be no tolerance. When 90 – 100% passing is designated, 90% shall be the minimum; no tolerance shall be used. 2These tolerances apply to the Contractor’s Quality Control Testing. |