January 17, 2008

REVISION OF SECTION 702

BITUMINOUS MATERIALS

NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction  It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions for its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by CDOT’s Standards and Specifications Unit.  The instructions for use on CDOT construction projects appear below.

Other agencies which use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use on projects having bituminous materials.

January 17, 2008

# 1

# REVISION OF SECTION 702

BITUMINOUS MATERIALS

# Section 702 of the Standard Specifications is hereby deleted for this project and replaced with the following:

702.01  Asphalt Cements.

(a)	Superpave Performance Graded Binders.  Superpave Performance Graded Binders shall conform to the requirements listed in Table 702-1.  (Taken from AASHTO M 320)

Asphalt cement shall not be acid modified or alkaline modified.

Asphalt cement shall not contain any used oils that have not been rerefined.  Modifiers that do not comply with environmental rules and regulations including 40 CFR Part 261.6(a) (3) (IV), and part 266/Subpart C shall not be added.  Modifiers shall not be carcinogenic.

The supplier of the PG binder shall be certified in accordance with CP 11.

January 17, 2008

# 2

# REVISION OF SECTION 702

BITUMINOUS MATERIALS

# Table 702-1

SUPERPAVE PERFORMANCE GRADED BINDERS

| Property | Requirement for PG Binder | AASHTO Test No. |
| --- | --- | --- |
|  | 58-28 | 58-34 | 64-22 | 64-28 | 76-28 |  |
| Original Binder Properties |  |  |  |  |  |  |
| Flash Point Temp., °C, minimum | 230 | 230 | 230 | 230 | 230 | T 48 |
| Viscosity at 135 °C, Pa●s, maximum | 3 | 3 | 3 | 3 | 3 | T 316 |
| Dynamic Shear, Temp. °C, where G*/Sin δ @ 10 rad/s ≥ 1.00 kPa | 58 | 58 | 64 | 64 | 76 | T 315 |
| Ductility, 4 °C (5 cm/min.), cm minimum | - | - | - | 50 | - | T 51 |
| Toughness, joules (inch-lbs) | - | - | - | 12.4 (110) | - | CP-L 2210 |
| Tenacity, joules (inch-lbs) | - | - | - | 8.5 (75) | - | CP-L 2210 |
| Acid or Alkali Modification (pass-fail) | Pass | Pass | Pass | Pass | Pass | CP-L 2214 |
| RTFO Residue Properties |  |  |  |  |  | CP-L 2215 |
| Mass Loss, percent maximum | 1.00 | 1.00 | 1.00 | 1.00 | 1.00 | CP-L 2215 |
| Dynamic Shear, Temp. °C, where G*/Sin δ @ 10 rad/s ≥ 2.20 kPa | 58 | 58 | 64 | 64 | 76 | T 315 |
| Elastic Recovery, 25 °C, percent min. | - | - | - | - | 50 | T 301 |
| Ductility, 4 °C (5 cm/min.), cm minimum | - | - | - | 20 | - | T 51 |
| PAV Residue Properties, Aging Temperature 100 °C |  |  |  |  |  | R 28 |
| Dynamic Shear, Temp. °C, where G*●Sin δ @ 10 rad/s ≤ 5000 kPa | 19 | 16 | 25 | 22 | 28 | T 315 |
| Creep Stiffness, @ 60 s, Test Temperature in °C | -18 | -24 | -12 | -18 | -18 | T 315 |
| S, maximum, MPa | 300 | 300 | 300 | 300 | 300 | T 313 |
| m-value, minimum | 0.300 | 0.300 | 0.300 | 0.300 | 0.300 | T 313 |
| **Direct Tension, Temperature in °C, @ 1 mm/min., where failure strain ≥ 1.0 % | -18 | -24 | -12 | -18 | -18 | T 314 |
| **Direct tension measurements are required when needed to show conformance to AASHTO M 320. |

January 17, 2008

# 3

# REVISION OF SECTION 702

BITUMINOUS MATERIALS

Acceptance Samples of the PG binder will be taken on the project in accordance with the Schedule in the Field Materials Manual.

The Department will test for acid modification and alkaline modification during the binder certification process.  Thereafter, the Department will randomly test for acid modification and alkaline modification.

(b)	Dampproofing.  Asphalt for damp proofing shall conform to the requirements of ASTM D 449, and the asphaltic primer shall conform to the requirements of ASTM D 41.

702.02  Liquid Asphaltic Materials.  Liquid asphaltic materials shall conform to the requirements of AASHTO M 81, M 82, and ASTM D 2026 for the designated types and grades.

702.03   Emulsified Asphalts.  Emulsified asphalts shall conform to AASHTO M 140 or M 208 for the designated types and grades. Emulsified asphalt and aggregate used for seal coats shall be sampled and will be tested for information only in accordance with CP-L 2213.

When grade CSS-1h or SS-1h emulsified asphalt is used for tack coat, residue penetration test values shall be 40 to 120.

Emulsified asphalt (HFMS-2S) with a residual penetration greater than 300 dmm shall conform to all properties listed in AASHTO M 140, Table 1 except that ductility shall be reported for information only.

- Emulsion for Seal Coat.  Polymerized emulsions for seal coat shall conform to the requirements listed in Table 702-2.   Emulsion for seal coat shall be an emulsified blend of polymerized asphalt, water, and emulsifiers. The asphalt cement shall be polymerized prior to emulsification and shall contain at least 3 percent polymer by weight of asphalt cement.  The emulsion standing undisturbed for a minimum of 24 hours shall show no white, milky separation but shall be smooth and homogeneous throughout.  The emulsion shall be pumpable and suitable for application through a distributor.

January 17, 2008

# 4

# REVISION OF SECTION 702

BITUMINOUS MATERIALS

Table 702-2

POLYMERIZED EMULSIONS FOR SEAL COATS

| Property | CRS-2P | CMS-2P | HFRS-2P | HFMS-2P | AASHTO Test No. |
| --- | --- | --- | --- | --- | --- |
| Tests on Emulsion: |  |  |  |  |  |
| Viscosity, at 50 ºC, Saybolt- Furol, s | min | 50 | 50 | 50 | 50 | T 59 |
|  | max | 450 | 450 | 450 | 450 |  |
| Storage stability, 24 hr, % max | 1.0 | 1.0 | 1.0 | 1.0 | T 59 |
| Particle charge test | Positive | Positive |  |  | T 59 |
| Sieve test, % max | 0.10 | 0.10 | 0.10 | 0.10 | T 59 |
| Demulsibility1, % min | 40 |  | 40 |  | T 59 |
| Oil Distillate by volume, % max or range | 3.0 | 3.0 | 3.0 | 3.0 | T-59 |
| Residue by distillation/ evaporation, % min3 | 653 | 653 | 653 | 653 | T 59/ CP-L 22122 |
| Tests on residue: |  |  |  |  |  |
| Penetration, 25 ºC, 100g, 5s, min, dmm | 70 | 70 | 70 | 70 | T 49 |
| Penetration, 25 ºC, 100g, 5s, max, dmm | 150 | 150 | 150 | 150 |  |
| Ductility, 25 ºC, 5 cm/min, cm, min |  |  | 75 | 75 | T 51 |
| Solubility, in trichloroethylene% min | 97.5 | 97.5 | 97.5 | 97.5 | T 44 |
| Elastic Recovery, 25 ºC min |  |  | 58 | 58 | T 301 |
| Float Test, 60 ºC, s min |  |  | 1200 | 1200 | T 50 |
| Toughness, in-lbs, min | 70 | 70 |  |  | CP-L 2210 |
| Tenacity, in-lbs, min | 45 | 45 |  |  | CP-L 2210 |
| 1If successful application is achieved in the field, the Engineer may wave this requirement. 2 CP-L 2212 is a rapid evaporation test for determining percent residue of an emulsion and providing material for tests on residue. CP-L 2212 is for acceptance only. If the percent residue or any test on the residue fails to meet specifications, the tests will be repeated using the distillation test in conformance with AASHTO T-59 to determine acceptability. 3 For polymerized emulsions the distillation and evaporation tests will in be in conformance with AASHTO T-59 or CP-L 2212 respectively with modifications to include 205 ± 5 ºC (400 ± 10 ºF) maximum temperature to be held for 15 minutes. |

# January 17, 2008

# 5

# REVISION OF SECTION 702

# BITUMINOUS MATERIALS

(b)	Emulsion for Prime Coat.  Emulsion for prime coat shall conform to the requirements of Table 702-3. Circulate before use if not used within 24 hours.

| Table 702-3 Asphalt EmulsionFOR Prime COAT |
| --- |
| Property | Requirement | AASHTO Test No. |
| Viscosity, Saybolt Furol, at 50 °C (122 °F), s | 20-150 | T 59 |
| % Residue | 65% min. | T 59 to 260 °C (500 °F) |
| Oil Distillate by Volume, % | 7% max. | T59 |
| Tests on Residue from Distillation: |  |  |
| Solubility in Trichloroethylene, % | 97.5 min. | T 44 |

(c)	Recycling Agent.  Recycling Agent for Item 406, Cold Bituminous Pavement (Recycle), shall be either a high float emulsified asphalt (polymerized) or an emulsified recycling agent as follows:

1.	High Float Emulsified Asphalt (Polymerized).  High Float Emulsified Asphalt (Polymerized) for Cold Bituminous Pavement (Recycle) shall be an emulsified blend of polymer modified asphalt, water, and emulsifiers conforming to Table 702-4 for HFMS-2sP.  The asphalt cement shall be polymerized prior to emulsification, and shall contain at least 3 percent polymer.

The emulsion standing undisturbed for a minimum of 24 hours shall show no white, milky separation, and shall be smooth and homogeneous throughout.

The emulsion shall be pumpable and suitable for application through a pressure distributor.

January 17, 2008

# 6

# REVISION OF SECTION 702

BITUMINOUS MATERIALS

# Table 702-4

HIGH FLOAT EMULSIFIED ASPHALT

(POLYMERIZED) (HFMS-2sP)

| Property | Requirement | AASHTO Test |
| --- | --- | --- |
|  | Minimum | Maximum |  |
| Tests on Emulsion: |  |  |  |
| Viscosity, Saybolt Furol at 50 °C (122 °F), sec | 50 | 450 | T 59 |
| Storage Stability test, 24 hours, % |  | 1 | T 59 |
| Sieve test, % |  | 0.10 | T 59 |
| % Residue1 | 65 |  | T 59 |
| Oil distillate by volume, % | 1 | 7 | T 59 |
| Tests on Residue: |  |  |  |
| Penetration, 25 °C (77 °F), 100g, 5 sec | 150 | 3002 | T 49 |
| Float Test, 60 °C (140 °F), sec | 1200 |  | T 50 |
| Solubility in TCE, % | 97.5 |  | T 44 |
| Elastic Recovery, 4 °C (39.2 °F), % | 50 |  | T 301 |
| 1400 ± 10° F maximum temperature to be held for 15 minutes. 2When approved by the Engineer, Emulsified Asphalt (HFMS-2sP) with a residual penetration greater than 300 dmm may be used with Cold Bituminous Pavement (Recycle) to address problems with cool weather or extremely aged existing pavement. Emulsified Asphalt (HFMS-2sP) with a residual penetration greater than 300 dmm shall meet all properties listed in Table 702-4 except that Elastic Recovery shall be reported for information only. |

- Emulsified Recycling Agent.  Emulsified Recycling Agent for use in Cold Bituminous Pavement (Recycle) shall conform to the requirements in Table 702-5.

January 17, 2008

# 7

# REVISION OF SECTION 702

# BITUMINOUS MATERIALS

# Table 702-5

EMULSIFIED RECYCLING AGENT

| Property | Requirement | Test |
| --- | --- | --- |
|  | Minimum | Maximum |  |
| Tests on Emulsion: |  |  |  |
| Viscosity @ 25 °C, SFS | 20 | 200 | ASTM D 244 |
| Pumping Stability | Pass |  | GB Method1 |
| Sieve Test, %w |  | 0.1 | ASTM D 2442 |
| Cement Mixing, %w |  | 2.0 | ASTM D 244 |
| Particle Charge | Positive |  | ASTM D 244 |
| Conc. Of Oil Phase | 64 |  | ASTM D 2443 |
| Tests on Residue: |  |  |  |
| Viscosity @ 60 °C , CST | 2000 | 4000 | ASTM D 2170 |
| Flash Point, COC, °C (° F) | 232 |  | ASTM D 92 |
| Maltenes Dist. PC+A1 Ratio4 S+A2 | 0.3 | 0.6 | ASTM D 2006 |
| PC/S Ratio | 0.4 |  | ASTM D 2006 |
| Asphaltenes, % max. |  | 11.0 | ASTM D 2006 |
| 1Pumping stability is determined by charging 450 ml of emulsion into a one liter beaker and circulating the emulsion through a gear pump (Roper 29.B22621) having a 6.3 mm (1/4 inch) inlet and outlet. The emulsion passes if there is no significant separation after circulating ten minutes. 2Test procedure identical with ASTM D 244 except that distilled water shall be used in place of 2 percent sodium oleate solution. 3ASTM D 244 Evaporation Test for percent of residue is modified by heating 50 gram sample to 149°C (300 °F) until foaming ceases, then cooling immediately and calculating results. 4In the Maltenes Distribution Ratio Test by ASTM Method D 2006. PC = Polar Compounds S = Saturates A1 = First Acidaffin A2 = Second Acidaffins |

# January 17, 2008

# 8

# REVISION OF SECTION 702

# BITUMINOUS MATERIALS

702.04  Asphalt Rejuvenating Agents.  Asphalt rejuvenating agents (ARA) shall be composed of a petroleum resin-oil base uniformly emulsified with water and shall conform to the physical and chemical requirements of Table 702-6 or ASTM D 4552.

| Table 702-6 Asphalt Rejuvenating Agent |
| --- |
| Property | Test Method | Requirement |
| Viscosity, S.F., @ 25 °C (77 °F), s | ASTM D 244 | 20-40 |
| 1Residue, % min. | ASTM D 244 | 60-65 |
| 2Miscibility Test | ASTM D 244 | No coagulation |
| 3Sieve Test, % max. | ASTM D 244 | 0.10 |
| Particle Charge Test | ASTM D 244 | Positive |
| ASTM D244 (Mod): |  |  |
| Viscosity, 60 °C (140 °F), mm2/s | ASTM D 445 | 100 - 200 |
| Flash Point, COC, °C, min. | ASTM D 92 | 196 |
| Asphaltenes, % max. | ASTM D2006 | 1.0 |
| 4Maltenes Dist. PC+A1 Ratio S+A2 | ASTM D 2006 | 0.3-0.6 |
| Saturated Hydrocarbons, % | ASTM D 2006 | 21-28 |
| 1 ASTM D244 Modified Evaporation Test for percent of residue is made by heating 50-gram sample to 149 °C (300 °F) until foaming ceases, then cooling immediately and calculating results. 2 Test procedure identical with ASTM D244 except that 0.02 Normal Calcium Chloride solution shall be used in place of distilled water. 3 Test procedure identical with ASTM D244 except that distilled water shall be used in place of 2% sodium oleate solution. 4 In the Maltenes Distribution Ratio Test by ASTM Method D4124: PC = Polar Compounds S = Saturates A1 = First Acidaffin A2 = Second Acidaffins |

For hot-in-place recycling ARA-1P is an acceptable alternative to ARA.  ARA-1P shall meet the requirements below:

Emulsified Polymer Modified Asphalt Rejuvenating Agent (ARA-1P) for use in hot-in-place recycling of bituminous pavements shall be modified with a minimum of 1.5 percent styrene-butadiene solution polymer. The finished product shall conform to the physical requirements listed in Table 702-7 below.

January 17, 2008

# 9

# REVISION OF SECTION 702

# BITUMINOUS MATERIALS

# Table 702-7

ARA-1P

| Property | Test Method | Min | Max |
| --- | --- | --- | --- |
| Test on Emulsion |  |  |  |
| Viscosity, Saybolt-Furol @ 77 ºF, s | ASTM D 244 |  | 100 |
| Residue @ 350 ºF, % | ASTM D 244 Mod | 60 |  |
| Sieve Test, % | ASTM D 244 |  | 0.10 |
| Oil distillate, % | ASTM D 244 |  | 2.0 |
| Test on Residue |  |  |  |
| Penetration @ 39.2 ºF, 100g, 5s, dmm | ASTM D-5 Modified | 150 | 250 |
| Asphaltenes, % | ASTM D 4124 |  | 15 |

702.05   (unused)

702.06  Hot Poured Joint and Crack Sealant.  Hot poured material for filling joints and cracks shall conform to the requirements of ASTM D 6690, Type I or II. The concrete blocks used in the Bond Test shall be prepared in accordance with CP-L 4101.

Sealant material shall be supplied preblended, prereacted, and prepackaged. If supplied in solid form the sealant material shall be cast in a plastic or other dissolvable liner having the capability of becoming part of the crack sealing liquid. The sealant shall be delivered in the manufacturer's original sealed container.

Each container shall be legibly marked with the manufacturer's name, the trade name of the sealer, the manufacturer's batch or lot number, the application temperature range, the recommended application temperature, and the safe heating temperature.

# The sealant shall be listed in CDOT’s Approved Products List prior to use.

January 17, 2008

# 10

# REVISION OF SECTION 702

# BITUMINOUS MATERIALS

## Colorado Procedure – Laboratory CP-L 4101

### Standard Practice for

## Preparing Concrete Blocks for Testing Sealants,

## for Joints and Cracks

ASTM Designation: D 1985-03

NOTE: Replace Subsections 5.1, 5.1.1, and 5.2 of ASTM D 1985-03 with the following:

  - Prepare the concrete in accordance with the procedure described in Test Method C 192/C102M using the following mix design:

Concrete Mix Proportions for 1 Cubic Yard SSD Batch Weight

Cement, Type I/II                      528 lb

Flyash, Class F                        132 lb

Coarse Aggregate,

Morrison Quarry, #57/67          1750 lb

Sand, Thornton Pit,

Washed Sand                         1100 lb

Note:   Contact Aggregate Industries at 303.777.2592 to obtain the aggregates.

5.2.   Use a metal or plastic mold provided with a metal or plastic base plate.  Provide means for securing the base plate to the mold.  Make the assembled mold and base plate water-tight and oil with mineral oil before use.  Fill the mold with concrete prepared in accordance with 5.1 to overflowing and vibrate externally for 30 s.   Screed (level) the concrete to a smooth surface with a wooden float and level off with a metal straightedge drawn across the top with a sawing motion.  Cure as specified in Test Method C 192/C 192M.  After curing for not less than 14 days, cut the slab of concrete into individual blocks using a 40 by 60-grit diamond saw blade rotating at a peripheral speed of 3050 ± 150 m/min. (10 000 ± 500 ft/min.).  Each test block should be 25 by 50 by 75 mm (1 by 2 by 3-in.).  Any face contacting the test material must be saw cut.  While the blocks are still wet from the sawing operation, scrub the surfaces of the blocks lightly with a non-metallic stiff-bristle brush while holding under a stream of running water.  Stocks of prepared blocks may be stored under standard conditions indefinitely, but store such blocks in a 100% humidity environment for not less than 7 days prior to use.