July 30, 2009

# REVISION OF SECTION 412

CONCRETE PAVEMENT JOINTS

## E

##### NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction.  It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions regarding its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by the Standards and Specifications Unit of the Project Development Branch.  The instructions for use on CDOT construction projects appear below.

Other agencies that use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use this standard special provision on projects having portland cement concrete pavement.

July 30, 2009

REVISION OF SECTION 412

CONCRETE PAVEMENT JOINTS

Section 412 of the Standard Specifications is hereby revised for this project as follows:

Subsection 412.13, first paragraph, shall include the following:

When a joint is saw cut more than 3 inches from the designated location, the pavement shall be removed and replaced to the nearest correct joints.  When portions of concrete pavement are removed and replaced, the portion removed shall be the full width of the lane and length of the affected slabs.  This corrective action shall be at the Contractor’s expense.

Delete Subsection 412.13(a)2., first paragraph, and replace with the following:

Transverse Construction Joints. Transverse construction joints shall be constructed as specified in the Contract. Transverse construction joints shall be constructed when the concrete placement is interrupted for more than 30 minutes and initial set is imminent. No transverse joint shall be constructed within 6 feet of another transverse joint. If sufficient concrete has not been mixed at the time of interruption to form a slab at least 6 feet long, the concrete back to the preceding joint shall be removed and the bulkhead placed in accordance with the requirements for a standard transverse contraction joint.

Subsection 412.13(b)2., first paragraph, shall include the following:

Horizontal support wires or shipping braces shall be non-deformed bars or wires with a diameter less than or equal to 0.307 inches (gauge 0 wire).  The number of horizontal support wires or shipping braces shall be limited to five per assembly.  The horizontal support wires or shipping braces shall not be cut prior to concrete placement.