November 5, 2009

REVISION OF SECTIONS 601 AND 701

STRUCTURAL CONCRETE

NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction.  It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions for its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by CDOT’s Standards and Specifications Unit.  The instructions for use on CDOT construction projects appear below.

Other agencies which use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use this special provision in projects having any type of concrete construction.

Designers will include a general note on the plans that states the sulfate level for the project.

Sections 601 and 701 of the Standard Specifications are hereby revised for this project as follows:

Delete subsection 601.02 and replace with the following:

601.02 Classification.  The classes of concrete shown in Table 601-1 shall be used when specified in the Contract.

Table 601-1

Concrete Table

| Concrete Class | Required Field Compressive Strength (psi) | Cementitious Content: Minimum or Range (lbs/yd3) | Air Content: % Range (Total) | Water Cementitious Ratio: Maximum or Range |
| --- | --- | --- | --- | --- |
| B | 4500 at 28 days | N/A | 5 - 8 | 0.45 |
| BZ | 4000 at 28 days | 610 | N/A | 0.45 |
| D | 4500 at 28 days | 615 to 660 | 5 – 8 | 0.45 |
| DT | 4500 at 28 days | 700 | 5 – 8 | 0.44 |
| E | 4200 at 28 days | 660 | 4 – 8 | 0.44 |
| H | 4500 at 56 days | 580 to 640 | 5 – 8 | 0.38 - 0.42 |
| HT | 4500 at 56 days | 580 to 640 | 5 – 8 | 0.38 - 0.42 |
| P | 4200 at 28 days | 660 | 4 – 8 | 0.44 |
| S35 | 5000 at 28 days | 615 to 720 | 5 – 8 | 0.42 |
| S40 | 5800 at 28 days | 615 to 760 | 5 – 8 | 0.40 |
| S50 | 7250 at 28 days | 615 to 800 | 5 – 8 | 0.38 |

Class B concrete is an air entrained concrete for general use.  Class D, H or P concrete may be substituted for Class B concrete.  Additional requirements are:  The coarse aggregate shall have a nominal maximum size of 1½ inches or smaller.

Class BZ concrete is concrete for drilled piers.  Additional requirements are:  Entrained air is not required unless specified in the Contract.  When entrained air is specified in the Contract, the air content shall be 5-8 percent.  High range water reducers may be added to obtain desired slump and retardation.  Slump shall be a minimum of 5 inches and a maximum of 8 inches.  The concrete mix shall be made with AASHTO M 43 size No. 67, No. 7 or No. 8 coarse aggregate.

Class D concrete is a dense medium strength structural concrete.  Class H may be substituted for Class D concrete.  Additional requirements are: An approved water reducing admixture shall be incorporated in the mix.  The concrete mix shall be made with AASHTO M 43 sizes No. 57, No. 6 or No. 67 coarse aggregate. When placed in a bridge deck, the concrete mix shall consist of a minimum 55 percent AASHTO M 43 size No. 67 coarse aggregate by weight of total aggregate.

Class DT concrete may be used for deck resurfacing and repairs.  Class HT may be substituted for Class DT concrete.  Additional requirements are:  An approved water reducing admixture shall be incorporated in the mix.  The concrete mix shall consist of a minimum 50 percent AASHTO M 43 size No. 7 or No. 8 coarse aggregate by weight of total aggregate.

Class E concrete may be used for fast track pavements needing early strength in order to open a pavement to service soon after placement.  Additional requirements are:  Type III cement may be used  The concrete mix shall consist of a minimum 55 percent AASHTO M 43 size No. 357 or No. 467 coarse aggregate by weight of total aggregate.  If all transverse joints are doweled, the concrete mix shall consist of a minimum 55 percent AASHTO M 43 sizes No. 57, No. 6, No. 67, No. 357, or No. 467 coarse aggregate by weight of total aggregate.  The laboratory trial mix shall produce a minimum average 28 day flexural strength of 650 psi. Class E concrete shall contain a minimum of 10 percent pozzolan by weight of total cementitious material.

Class H concrete is used for bare concrete bridge decks that will not receive a waterproofing membrane.  Additional requirements are:  An approved water reducing admixture shall be incorporated in the mix.  The concrete mix shall consist of a minimum of 55 percent AASHTO M 43 size No. 67 coarse aggregate by weight of total aggregate.  Class H concrete shall contain cementitious materials in the following ranges:  450 to 500 pounds per cubic yard Type II portland cement, 90 to 125 pounds per cubic yard fly ash and 20 to 30 pounds per cubic yard silica fume.  The total content of Type II portland cement, fly ash and silica fume shall be 580 to 640 pounds per cubic yard.  The laboratory trial mix must not exceed permeability of 2000 coulombs at 56 days (ASTM C 1202) and must not exhibit a crack at or before 14 days in the cracking tendency test (AASHTO T334).

Class HT concrete is used as the top layer for bare concrete bridge decks that will not receive a waterproofing membrane.  Additional requirements are:  An approved water reducing admixture shall be incorporated in the mix.  The concrete mix shall consist of a minimum of 50 percent AASHTO M 43 size No. 7 or No. 8 coarse aggregate by weight of total aggregate.  Class HT concrete shall contain cementitious materials in the following ranges:  450 to 500 pounds per cubic yard Type II portland cement, 90 to 125 pounds per cubic yard fly ash and 20 to 30 pounds per cubic yard silica fume.  The total content of Type II portland cement, fly ash and silica fume shall be 580 to 640 pounds per cubic yard.  The laboratory trial mix must not exceed permeability of 2000 coulombs at 56 days (ASTM C 1202) and must not exhibit a crack at or before 14 days in the cracking tendency test (AASHTO T334).

Class P concrete is used in pavements.  Additional requirements are:  The concrete mix shall consist of a minimum 55 percent AASHTO M 43 size No. 357 or No. 467 coarse aggregate by weight of total aggregate.  If all transverse joints are doweled, the concrete mix shall consist of a minimum 55 percent AASHTO M 43 sizes No. 57, No. 6, No. 67, No. 357, or No. 467 coarse aggregate by weight of total aggregate.  The laboratory trial mix shall produce a minimum average 28 day flexural strength of 650 psi.  Class P concrete shall contain a minimum of 10 percent pozzolan by weight of total cementitious.  If acceptance is based on flexural strength, the total weight of cementitious shall not be less than 520 pounds per cubic yard.

Class S35 concrete is a dense high strength structural concrete.  Additional requirements are:  An approved water reducing admixture shall be incorporated in the mix.  The concrete mix shall be made with AASHTO M 43 sizes No. 57, No. 6, No. 67, No. 7 or No. 8 coarse aggregate. When placed in a bridge deck, the concrete mix shall consist of a minimum 55 percent AASHTO M 43 size No. 67 coarse aggregate by weight of total aggregate.

Class S40 concrete is a dense high strength structural concrete.  Additional requirements are:  An approved water reducing admixture shall be incorporated in the mix.  The concrete mix shall be made with AASHTO M 43 sizes No. 57, No. 6, No. 67, No. 7 or No. 8 coarse aggregate.  When placed in a bridge deck, the concrete mix shall consist of a minimum 55 percent AASHTO M 43 size No. 67 coarse aggregate.

Class S50 concrete is a dense high strength structural concrete.  Additional requirements are:  An approved water reducing admixture shall be incorporated in the mix.  The concrete mix shall be made with AASHTO M 43 sizes No. 57, No. 6, No. 67, No. 7 or No. 8 coarse aggregate.  When placed in a bridge deck, the concrete mix shall consist of a minimum 55 percent AASHTO M 43 size No. 67 coarse aggregate by weight of total aggregate.

The laboratory trial mix must not exhibit a crack at or before 14 days in the cracking tendency test (AASHTO T334).

Subsection 601.04 shall include the following:

601.04 Sulfate Resistance.  The Contractor shall provide protection against sulfate attack on concrete structures and pavements by providing concrete manufactured with requirements according to Table 601-4.  The sulfate exposure for all concrete shall be Class 2 unless otherwise stated on the plans.  A higher level of requirements may be used for a lower level of exposure.

If the Contractor can provide a test report that shows another class of exposure exists at a structure location, then the Engineer may accept a concrete mix for that location that meets the corresponding sulfate protection requirements in addition to other requirements shown in this section.

Table 601-4

REQUIREMENTS TO PROTECT AGAINST DAMAGE TO

CONCRETE BY SULFATE ATTACK FROM EXTERNAL SOURCES OF SULFATE

| Severity of sulfate exposure | Water-soluble sulfate (SO4) in dry soil, percent, | Sulfate (SO4) in water, ppm | Water cementitious ratio, maximum | Cementitious material requirements |
| --- | --- | --- | --- | --- |
| Class 0 | 0.00 to 0.10 | 0 to 150 | 0.45 | Class 0 |
| Class 1 | 0.11 to 0.20 | 151 to 1500 | 0.45 | Class 1 |
| Class 2 | 0.21 to 2.00 | 1501 to 10,000 | 0.45 | Class 2 |
| Class 3 | 2.01 or greater | 10,001 or greater | 0.40 | Class 3 |

Cementitious material requirements are as follows:

Class 0 requirements for sulfate resistance shall be one of the following:

- ASTM C 150 Type I, II or V

- ASTM C 595 Type IP, IP(MS) or IP(HS)

- ASTM C 1157 Type GU, MS or HS

- ASTM C 150 Type III cement if it is allowed, as in Class E concrete

Class 1 requirements for sulfate resistance shall be one of the following:

- ASTM C 150 Type II or V; Class C fly ash shall not be substituted for cement

- ASTM C 595 Type IP(MS) or IP(HS); Class C fly ash shall not be substituted for cement.

- ASTM C 1157 Type MS or HS; Class C fly ash shall not be substituted for cement.

- When ASTM C 150 Type III cement is allowed, as in Class E concrete, it shall have no more than 8 percent C3A. Class C fly ash shall not be substituted for cement

Class 2 requirements for sulfate resistance shall be one of the following:

- ASTM C 150 Type V with a minimum of a 20 percent substitution of Class F fly ash by weight

- ASTM C 150 Type II or III with a minimum of a 20 percent substitution of Class F fly ash by weight.  The Type II or III cement shall have no more than 0.040 percent expansion at 14 days when tested according ASTM C 452

- ASTM C 1157 Type HS; Class C fly ash shall not be substituted for cement.

- ASTM C 1157 Type MS plus Class F fly ash where the blend has less than 0.05 percent expansion at 6 months or 0.10 percent expansion at 12 months when tested according to ASTM C 1012

- A blend of portland cement meeting ASTM C 150 Type II or III with a minimum of 20 percent Class F fly ash by weight, where the blend has less than 0.05 percent expansion at 6 months or 0.10 percent expansion at 12 months when tested according to ASTM C 1012.

- ASTM C 595 Type IP(HS); Class C fly ash shall not be substituted for cement.

Class 3 requirements for sulfate resistance shall be one of the following:

- A blend of portland cement meeting ASTM C 150 Type II, III, or V with a minimum of a 20 percent substitution of Class F fly ash by weight, where the blend has less than 0.10 percent expansion at 18 months when tested according to ASTM C 1012.

- ASTM C 1157 Type HS having less than 0.10 percent expansion at 18 months when tested according to ASTM C 1012.  Class C fly ash shall not be substituted for cement

- ASTM C 1157 Type MS or HS plus Class F fly ash where the blend has less than 0.10 percent expansion at 18 months when tested according to ASTM C 1012.

- ASTM C 595 Type IP(HS) having less than 0.10 percent expansion at 18 months when tested according to ASTM C 1012.  Class C fly ash shall not be substituted for cement.

When fly ash is used to enhance sulfate resistance, it shall be used in a proportion greater than or equal to the proportion tested in accordance to ASTM C1012, shall be the same source and it shall have a calcium oxide content no more than 2.0 percent greater than the fly ash tested according to ASTM 1012.

Delete subsection 601.05 and replace with the following:

601.05 Proportioning. The Contractor shall submit a Concrete Mix Design for each class of concrete being placed on the project.  Concrete shall not be placed on the project before the Concrete Mix Design Report has been reviewed and approved by the Engineer.  The Concrete Mix Design will be reviewed and approved following the procedures of CP 62.  The Concrete Mix Design will not be approved when the laboratory trial mix data are the results from tests performed more than two years in the past or aggregate data are the results from tests performed more than two years in the past.  The concrete mix design shall show the weights and sources of all ingredients including cement, pozzolan, aggregates, water, additives and the water cementitious ratio (w/cm).  When determining the w/cm, cementitious (cm) shall be the sum of the weight of the cement, the weight of the fly ash and the weight of silica fume.

The laboratory trial mix data shall include results of the following:

- AASHTO T 119 (ASTM C 143) Slump of Hydraulic Cement Concrete.

- AASHTO T 121 (ASTM C 138) Weight per Cubic Foot, Yield, and Air Content (Gravimetric) of Concrete.

- AASHTO T 152 (ASTM C 231) Air Content of Freshly Mixed Concrete by the Pressure Method

- ASTM C 39 Compressive Strength of Cylindrical Concrete Specimens shall be performed with at least two specimens at 7 days and three specimens at 28 days.  Three additional specimens tested at 56 days shall be required for Class H and HT concrete.

- Class H and HT concrete shall include a measurement of permeability by ASTM C 1202 Electrical Indication of Concrete's Ability to Resist Chloride Ion Penetration.  The concrete test specimens shall be two 2 inch thick disks sawed from the centers of two molded 4 inch diameter cylinders cured 56 days in accordance with ASTM C 192 Standard Practice for Making and Curing Concrete Test Specimens in the Laboratory.

- Class H, HT and S50 concrete shall include a measurement of cracking by AASHTO T334 Standard Practice for Estimating the Cracking Tendency of Concrete.  The sample shall be cured at a temperature of 65 to 75 F and relative humidity not exceeding 40 percent.

- Class E and P concrete shall include AASHTO T 97 (ASTM C 78) Flexural Strength of Concrete (Using Simple Beam with Third-Point Loading) performed with at least two specimens at seven days and four specimens at 28 days.

Prior to placement of Class E concrete, the Contractor shall provide the Engineer a report of maturity relationships in accordance with CP 69.  The Contractor shall provide maturity meter and all necessary wire and connectors.

The Contractor shall be responsible for the placement and maintenance of the maturity meter and wire.  Placement shall be as directed by the Engineer.

Except for class BZ concrete, the maximum slump of the delivered concrete shall be the slump of the approved concrete mix design plus 1½ inch.  Except for class H and HT concrete, the laboratory trial mix must produce an average 28 day compressive strength at least 115 percent of the required 28 day field compressive strength.  The laboratory trial mix for Class H or HT concrete must produce an average 56 day compressive strength at least 115 percent of the required 56 day field compressive strength.

When entrained air is specified in the Contract for Class BZ concrete, an air entraining admixture may be added to an approved Class BZ mix design.  A new trial mix will not be required.

The laboratory trial mix shall have a relative yield of 0.99 to 1.02.  When Portland Cement Concrete Pavement is paid with a volumetric pay quantity, the relative yield of the concrete produced on the project shall be 0.99 to 1.02.

If the produced concrete does not have a relative yield of 0.99 to 1.02 for two consecutive yield determinations, concrete production shall cease and the Contractor shall present a plan to correct the relative yield to the Engineer.

Aggregate data shall include the results of the following:

- AASHTO T 11 (ASTM C 117) Materials Finer Than 75 um (No. 200) Sieve in Mineral Aggregates by Washing.

- AASHTO T 19 (ASTM C 29) Unit Weight and Voids in Aggregate.

- AASHTO T 21 (ASTM C 40) Organic Impurities in Fine Aggregate for Concrete.

- AASHTO T 27 (ASTM C 136) Sieve Analysis of Fine and Coarse Aggregates.

- AASHTO T 84 (ASTM C 128) Specific Gravity and Absorption of Fine Aggregate.

- AASHTO T 85 (ASTM C 127) Specific Gravity and Absorption of Coarse Aggregate.

- AASHTO T 96 (ASTM C 131) Resistance to Degradation of Small-Size Coarse Aggregate by Abrasion and Impact in the Los Angeles Machine.

- AASHTO T 104 (ASTM C 88) Soundness of Aggregate by Use of Sodium Sulfate or Magnesium Sulfate.

- CP 37 Plastic Fines in Graded Aggregates and Soils by use of the Sand Equivalent Test

- ASTM C 535 Resistance to Degradation of Large-Size Coarse Aggregate by Abrasion and Impact in the Los Angeles Machine

- ASTM C1260 Determining the Potential Alkali Reactivity of Aggregates (Accelerated Mortar-Bar Method).  When an aggregate source is known to be reactive, ASTM C1567 results may be submitted in lieu of ASTM C1260 results.

Any aggregate tested by ASTM C1260 with an expansion of 0.10 percent or more, or that is known to be reactive, shall not be used unless mitigative measures are included in the mix design.

Test results from ASTM C1293 Standard Test Method for Determination of Length Change of Concrete Due to Alkali-Silica Reaction may be substituted for ASTM C1260 test results.  The ASTM C1293 test shall be run on an individual source of aggregate.  The ASTM C1293 test shall not use fly ash or slag as part of the cementitious content.  Any aggregate source tested by ASTM C1293 with an expansion greater than or equal to 0.04 percent at one year shall not be used unless mitigative measures are included in the mix design.

Mitigative measures shall be tested using ASTM C1567 and exhibit an expansion less than 0.10 percent by one of the following methods:

- Combined Aggregates.  The mix design sources of aggregates, cement and mitigative measures shall be tested. The proportions of aggregates and mitigative measures shall be those used in the mix design.

- Individual Aggregates.  Each source and size of individual aggregates shall be tested.  The source of cement and mitigative measures shall be those used in the mix design.  The highest level of mitigative measures for any individual aggregate shall be the minimum used in the mix design.

The Concrete Mix Design Report shall include Certified Test Reports showing that the cement, fly ash and silica fume meet the specification requirements and supporting this statement with actual test results.  The certification for silica fume shall state the solids content if the silica fume admixture is furnished as slurry.

Approved fly ash may be substituted for ASTM C150 cement up to a maximum of 20 percent Class C or 30 percent Class F by weight of total cementitious.

For all concrete mix designs with ASTM C595 or C1157 cements, the total pozzolan content shall not exceed 30 percent by weight of the cementitious content.

Where the Contractor’s use of fly ash results in any delay, necessary changes in admixture quantities or source, or unsatisfactory work, the cost of such delays, changes or corrective actions shall be borne by the Contractor.

The Contractor shall submit a new Concrete Mix Design Report meeting the above requirements when a change occurs in the source, type, or proportions of cement, fly ash, silica fume or aggregate.  When a change occurs in the source of approved admixtures, the Contractor shall submit a letter stamped by the Concrete Mix Design Engineer approving the changes to the existing mix design.  The change will be approved by the Engineer prior to use.

The use of approved accelerating, retarding or hydration stabilizing admixtures to existing mix designs will be permitted at the discretion of the Engineer when documentation includes the following:

- Manufacturers recommended dosage of the admixture

- A letter stamped by the Concrete Mix Design Engineer approving the changes to the existing mix design.

Unless otherwise permitted by the Engineer, the product of only one type of hydraulic cement from one source of any one brand shall be used in a concrete mix design.

Review and approval of the Concrete Mix Design by the Engineer does not constitute acceptance of the concrete.  Acceptance will be based solely on the test results of concrete placed on the project.

Subsection 601.12 (j), third paragraph, shall include the following:

When concrete is to be placed on or adjacent to hardened concrete surfaces, the surface shall be saturated surface dry.  Saturated surface dry concrete has no water on its surface.  The pores of the concrete beneath the surface are moist.

Delete subsection 701.01 and replace with the following:

701.01  Hydraulic Cement.  Hydraulic cement shall conform to the requirements of the following specifications for the type specified or permitted:

Portland Cement	ASTM C 150

Blended Hydraulic Cement	ASTM C 595

Hydraulic Cement	ASTM C 1157

All concrete, including precast, prestressed and pipe shall be constructed with one of the following hydraulic cements unless permitted otherwise.

ASTM C 150 Type I

ASTM C 150 Type II

ASTM C 150 Type V

ASTM C 595 Type IP consisting of no less than 70 percent portland cement,

ASTM C 595 Type IP(MS) consisting of no less than 70 percent portland cement,

ASTM C 595 Type IP(HS) consisting of no less than 70 percent portland cement,

ASTM C 1157 Type GU, consisting of no more than 10 percent limestone,

ASTM C 1157 Type MS, consisting of no more than 10 percent limestone,

ASTM C 1157 Type HS, consisting of no more than 10 percent limestone,

Cement shall be from a preapproved source listed on the Department’s Approved Products List.  The cement intended for use on the project shall have been tested and accepted prior to its use.  Certified Test Reports showing that the cement meets the specification requirements and supporting this statement with actual test results shall be submitted to the Engineer prior to the tested material being incorporated into the project.  Certified Test Reports shall indicate the percentage of pozzolan and/or limestone incorporated into the cement.

The cement shall be subject to sampling and testing by the Department.  Test results that do not meet the physical and chemical requirements may result in the suspension of the use of the cement until the corrections necessary have been taken to insure that the material meets the specifications.

The Contractor shall provide suitable means for storing and protecting the cement against dampness.  Cement which, for an reason, has become partially set or which contains lumps of caked cement shall not be used.

Cement salvaged from discarded or used bags shall not be used.

Delete subsection 701.02 and replace with the following:

701.02 Fly Ash. Fly ash for concrete shall conform to the requirements of ASTM C 618, Class C or Class F with the following exceptions:

- The loss on ignition shall not exceed 3.0 percent.

- The CaO in Class F fly ash shall not exceed 18 percent.

Fly ash shall be from a preapproved source listed on the Department’s Approved Products List. The fly ash intended for use on the project shall have been tested and accepted prior to its use. Certified Test Reports showing that the fly ash meets the specification requirements and supporting this statement with actual test results shall be submitted to the Engineer.

Preapproval shall include submission of a report from the supplier documenting the results of testing the fly ash from that source in accordance with the Toxicity Characteristic Leaching Procedure (TCLP) described in 40 CFR 261, Appendix II. The report shall include the results of TCLP testing for heavy metals and other contaminants found in the fly ash. The report shall list the contaminants tested, and the allowable levels for each contaminant tested. A new report shall be submitted for each preapproved source annually. Additional TCLP testing may be required when the Department suspects that the fly ash source may have been contaminated.

The fly ash shall be subject to sampling and testing by the Department. Test results that do not meet the physical and chemical requirements may result in the suspension of the use of fly ash until the corrections necessary have been taken to insure that the material meets the specifications.