Sample project special: 610mcmpc

11-05-09

REVISION OF SECTION 610

MEDIAN COVER MATERIAL (PATTERNED CONCRETE)

Section 610 of the Standard Specifications is hereby revised for this project as follows:

Subsection 610.02 shall include the following:

Patterned concrete shall be colored concrete and meet the requirements of Class B concrete with the following exceptions:

Slump, AASHTO T 119, inches						2 to 5

Coarse Aggregate, AASHTO M 43					No. 8

Fine Aggregate, AASHTO M 6, percent of

the total aggregate								50 to78

An approved water reducing admixture shall be used in the mix.

The coloring agent shall be either integral to the concrete mixture or applied by the dry shake method.

The color and pattern shall be as shown on the plans.  Color shall be approved by the Engineer.

Colored wax curing membrane shall be as recommended by the supplier of the coloring agent.

Subsection 610.03 shall include the following:

(d)	Patterned Concrete.  Construction shall conform to the requirements of subsection 608.03 with the following exceptions:

When the color is added by the dry shake method, the coloring agent shall be uniformly sifted over the plastic concrete.

While the concrete is still plastic, a special pattern forming tool shall be applied to the concrete surface to form the specified pattern.  All tears and voids resulting from the pattern forming shall be repaired.

Curing shall include application of two coats of colored wax curing membrane.  The first coat shall be applied within two hours of finishing.  The second coat shall be applied between 10 and 20 days following the first application.