2.25.2010

Project Special Worksheet: 603rcp

REVISION OF SECTION 603

REINFORCED CONCRETE PIPE

Section 603 of the Standard Specifications is hereby revised for this project as follows:

Subsection 603.02 shall include the following:

♦Reinforced concrete pipe shall be manufactured from concrete that meets the requirements for severity of sulfate exposure Class ♦ specified in subsection 601.04.

▲Reinforced concrete pipe shall be coated in accordance with subsection 706.07.

INSTRUCTIONS TO DESIGNERS (delete instructions and symbols from final draft):

Consult the CDOT Pipe Material Selection Policy before using this worksheet to develop a special provision for inclusion in the Contract.  Use this worksheet ONLY when use of a single pipe material is justified in accordance with the CDOT Pipe Material Selection Policy.  Otherwise, pay for the pipe using the Section 624 pay item of the appropriate class.

♦	Use this statement only when the Section 603 pay item reinforced concrete pipe is specified.  Insert the appropriate sulfate exposure class determined in accordance with the CDOT Pipe Material Selection Policy.

▲	Use this statement only when the Section 603 pay item reinforced concrete pipe is specified and the pH of the soil or water is less than 5.  See the CDOT Pipe Material Selection Policy.