2.25.10
Project Special Worksheet: 624dp

REVISION OF SECTION 624

DRAINAGE PIPE

Section 624 of the Standard Specifications is hereby revised for this project as follows:

Subsection 624.02 shall include the following:

▲Reinforced concrete pipe shall be coated in accordance with subsection 706.07.

♥ Joint systems for siphons, irrigation systems, and storm drains shall be watertight.

♦Aluminum alloy pipe shall not be used.

INSTRUCTIONS TO DESIGNERS (delete instructions and symbols from final draft):

Consult the CDOT Pipe Material Selection Policy before using this worksheet to develop a special provision for inclusion in the Contract.  If none of the following criteria apply to the Contract, a special provision based on this worksheet is not required.

▲	Use this statement when the specified class of pipe allows RCP and the pH of the soil or water is less than 5.  See the CDOT Pipe Material Selection Policy.

♥	Use this statement, or an appropriate variation thereof, when watertight joints are required.

♦	Use this statement when the specified class of pipe allows Aluminum alloy and the abrasion level is higher than 1. See the CDOT Pipe Material Selection Policy.