Section 213 of the Standard Specifications is hereby revised for this project as follows:

Subsection 213.01 shall include the following:

This work consists of furnishing and placing soil binder over soil on roadway ditches or slopes indicated on the plans or as designated.

Subsection 213.02 shall include the following:

Material for soil binder shall consist of a dry granular formula containing anionic polyacrylamide polymer.  Formulas containing neutral polyacrylamide polymers or cationic polyacrylamide polymers shall not be used.  The molecular weight of the polymer shall be between 12 and 20 mg/mole.

The material used for soil binder shall not contain any mineral filler, clays, or other substances which may inhibit germination or growth of plants.  Water shall conform to subsection 209.02. Wood cellulose fiber shall conform to subsection 213.02. The wood cellulose fiber used with the soil binder application may contain recycled wood fibers.

Subsection 213.03 (b) shall include the following:

3. Application of soil binder shall be done hydraulically in accordance with the following:

Application guidelines:

| Soil binder/acre | Water/acre | Fiber/acre |
| --- | --- | --- |
| 20 lbs. | 1000 gallons | 900 lbs. |

Mixing Procedure for Soil Binder:

- Fill tank with a minimum of one-third of the required volume of water.

- Run agitators at high speed while the soil binder is slowly added to the water.

- Add wood cellulose fiber. Agitate until homogenous, non-lumpy slurry is formed.

- Agitate for a minimum of ten minutes prior to application.

- Spray onto mulch or soil using a nozzle that will disperse the spray into slurry that will uniformly cover the surface.

Subsection 213.04 shall include the following:

Soil binder will be measured as the actual number of acres or the actual number of pounds that are applied and accepted.  The quantity of soil binder shall include water, fiber and soil binder applied in accordance with the foregoing requirements, completed and accepted.

Subsection 213.05 shall include the following:

Pay Item                                          Pay Unit

Soil binder                                        Acre

Soil binder                                        Pound

Water, mixing and application will not be measured and paid for separately but shall be included in the work.