October 31, 2013

REVISION OF SECTION 703

AGGREGATE FOR BASES

(WITHOUT RAP)

**NOTICE**

This is a standard special provision that revises or modifies CDOT’s *Standard Specifications for Road and Bridge Construction.* It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions for its use on CDOT construction projects. It is to be used as written without change. Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by CDOT’s Standards and Specifications Unit. The instructions for use on CDOT construction projects appear below.

Other agencies which use the *Standard Specifications for Road and Bridge Construction* to administer construction projects may use this special provision as appropriate and at their own risk.

**Instructions for use on CDOT construction projects:**

Use in projects which do not allow reclaimed asphalt pavement material (RAP) to be incorporated into the aggregate base course mix. The Designer should contact the Region Materials Engineer to determine use.

October 31, 2013

1

REVISION OF SECTION 703

AGGREGATE FOR BASES

(WITHOUT RAP)

Section 703 of the Standard Specifications is hereby revised for this project as follows:

In subsection 703.03, delete the first paragraph and replace with the following:

**703.03 Aggregate for Bases.** Aggregates for bases except Aggregate Base Course (RAP) shall be crushed stone, crushed slag, crushed gravel, natural gravel, or crushed reclaimed concrete. Aggregate Base Course (RAP) shall be 100 percent crushed recycled asphalt pavement material. All materials except Aggregate Base Course (RAP) shall conform to the quality requirements of AASHTO M 147 except that the requirements for the ratio of minus 75 µm (No. 200) sieve fraction to the minus 425 µm (No. 40) sieve fraction, stated in 3.2.2 of AASHTO M 147, shall not apply.

The requirements for the Los Angeles wear test (AASHTO T 96 & ASTM C535) shall not apply to Class 1, 2, and 3. Aggregates for bases shall meet the grading requirements of Table 703-3 for the class specified for the project, unless otherwise specified.