Sample project special: 405hst

02-03-11

Revision of Section 405

Heating and Scarifying Treatment

Section 405 of the Standard Specifications is hereby revised for this project to include the following:

Delete subsection 405.02 and replace with the following:

**405.02** **Asphalt Rejuvenating or Recycling Agent.**  Rejuvenating or recycling agent shall meet one of the following requirements:

1. Rejuvenating agent shall meet the requirements of subsection 702.04.

1. Recycling agent shall meet the requirements of Table 702-6, except that the residual penetration shall be greater than 300 dmm.

Subsection 405.03 shall include the following:

The Contractor shall protect the area adjacent to the work from heat damage. All damages to this area resulting from heat damage shall be repaired or replaced at the Contractor's expense. The Engineer may require the Contractor to furnish fire fighting equipment at the Contractor’s expense.

The Contractor shall meet all local, county, state, and federal air pollution regulations. All costs and extra work necessary to comply with air pollution regulations shall be at the Contractor’s expense.

Areas that ravel or pothole shall be repaired or patched at the Contractor's expense.

In subsection 405.05, delete the last sentence and replace with the following:

The rejuvenating or recycling agent will be measured and paid for in accordance with Section 411 under Pay Item 411, Asphalt Rejuvenating Agent.