Sample project special: 703abcs

02-03-11

REVISION OF SECTION 703

AGGREGATE BASE COURSE (SPECIAL)

Section 703 of the Standard Specifications is hereby revised for this project as follows:

Subsection 703.03 shall include the following:

The plasticity index for Aggregate Base Course (Special) shall be within the range of 3-15 when the aggregate is tested in accordance with AASHTO T-90.