May 2, 2013

REVISION OF SECTIONS 507, 601 AND 606

MACRO FIBER-REINFORCED CONCRETE

NOTICE

This is a standard special provision that revises or modifies CDOT’s Standard Specifications for Road and Bridge Construction. It has gone through a formal review and approval process and has been issued by CDOT’s Project Development Branch with formal instructions for its use on CDOT construction projects.  It is to be used as written without change.  Do not use modified versions of this special provision on CDOT construction projects, and do not use this special provision on CDOT projects in a manner other than that specified in the instructions unless such use is first approved by CDOT’s Standards and Specifications Unit.  The instructions for use on CDOT construction projects appear below.

Other agencies which use the Standard Specifications for Road and Bridge Construction to administer construction projects may use this special provision as appropriate and at their own risk.

Instructions for use on CDOT construction projects:

Use in projects having macro fiber-reinforced concrete.

May 2, 2013

REVISION OF SECTIONS 507, 601 AND 606 
MACRO FIBER-REINFORCED CONCRETE

Sections 507, 601 and 606 of the Standard Specifications are hereby revised for this project as follows:

Delete subsection 507.02 and replace with the following:

507.02 Concrete, Slope and Ditch Paving.  Concrete shall conform to the requirements of Section 601.  Concrete shall be Macro Fiber-Reinforced Class B Concrete.

Preformed joint filler shall conform to AASHTO M 213

In subsection 507.08, first paragraph, delete the second sentence.

Subsection 507.14 shall include the following:

Polyolefin fiber reinforcement will not be measured and paid for separately, but shall be included in the work.

Subsection 601.05 shall include the following:

Concrete for Bridge Sidewalk shall be Macro Fiber-Reinforced Class D Concrete

Subsection 606.02 shall include the following:

Concrete for bridge rail shall be Macro Fiber-Reinforced Class D Concrete and conform to the requirements of Section 601

Subsection 606.06 shall include the following:

Polyolefin fiber reinforcement will not be measured and paid for separately, but shall be included in the work.