Revise Section 703 of the standard specifications as follows:

Table 703-7 shall be replaced with the following:

**Table 703-7**

**GRADATION SPECIFICATIONS FOR COVER COAT AGGREGATE**

|  |  |  |  |
| --- | --- | --- | --- |
| **Sieve Size** | **Percent by Weight Passing Square Mesh Sieve** | | |
| **9.5 mm (3⁄8")**  **Type 1** | **12.5 mm (½") Type II** | **19.0 mm (¾")\* Type IV** |
| 19.0 mm (¾") |  |  | 100 |
| 12.5 mm (½") |  | 100 | 95-100 |
| 9.5 mm (3⁄8") | 100 | 65-85 | 60-80 |
| 4.75 mm (#4) | 0-15 | 0-10 | 0-10 |
| 75 μm (#200) | 0-1.5 | 0-1.5 | 0-1.5 |
| \*Type IV shall be used only with lightweight aggregates. | | | |