**Revise Section 627 of the Standard Specifications as follows:**

**Revise Table 627-1 of the Standard Specifications as follows:**

**Table 627-1**

## MINIMUM AND MAXIMUM RANGES OF PAINT AND STRIPES

|  |  |
| --- | --- |
| **Description** | **Pavement Marking Paint** |
| Low Temp | High Build | High Build(15 Mil)  |
| Alignment | Lateral Deviation | 2.0 inch per 200 feet Max |
| Coverage Rate | Sq Ft per Gallon | 89-94 | 67-70 | 100-105 |
| Thickness | Mil | 17-18 | 23-24 | 15-16 |
| Width | Inches | Per Plans ± 0.25 |
| Dry Time | Minutes | 5-10 | 7-12 | 5-10 |
| Beads | Application Rate, lbs./gal | 7-8 | 9-10 | 7-8 |

(6) High Build (15 Mil) shall only be used for temporary pavement marking applications.

**Add to Section 627.13 of the Standard Specifications as follows:**

**627.13** The accepted quantities will be paid for at the contract price per unit of measurement for each of the pay items listed below that appear in the bid schedule.

Payment will be made under:

**Pay Item** **Pay Unit**

High Build (15 Mil) Gallon