**Page 601-50, Table 601-3, “Deviations From Specified Air” was deleted erroneously.**

Table 601-3 Notes: \* Concrete represented by out-of-spec tests will only be price-reduced with the lowest pay factor, not for each pay factor.

|  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| **Below Specified Strength (psi) [ ≥ 4500 psi Concrete]** | \***Pay Factor (Percent)** |  | **Below Specified Strength (psi) [ < 4500 psi Concrete]** | \***Pay Factor (Percent)** |  | **Deviations From Specified Air (Percent)** | \***Pay Factor (Percent)** |
| 1 – 100 | 98 |  | 1 – 100 | 98 |  |
| 101 – 200 | 96 |  | 101 – 200 | 96 |  | 0.0 – 0.2 | 98 |
| 201 – 300 | 92 |  | 201 – 300 | 92 |  | 0.3 – 0.4 | 96 |
| 301 – 400 | 84 |  | 301 – 400 | 84 |  | 0.5 – 0.6 | 92 |
| 401 – 500 | 75 |  | 401 – 500 | 75 |  | 0.7 – 0.8 | 84 |
|  | Reject |  | Over 500 | Reject |  | 0.9 – 1.0 | 75 |
| 501 – 600 | 65 |  |  |  |  | Over 1.0 | Reject |
| 601 – 700 | 54 |  |  |  |  |  |  |
| 701 – 800 | 42 |  |  |  |  |  |  |
| 801 – 900 | 29 |  |  |  |  |  |  |
| 901 – 1000 | 15 |  |  |  |  |  |  |
| Over 1000 | Reject |  |  |  |  |  |  |