September 5, 2024

Revision of Section 508

Timber Structures

Revise Section 508 of the Standard Specifications as follows:

Revise Subsection 508.04 as shown:

  - Inspection. Sawn products that are pressure treated shall be tagged to indicate the AWPA U1 use category and include the quality mark of an American Lumber Standard Committee (ALSC) accredited agency. Sawn products not bearing the quality mark and Aall other timber products furnished shall be covered by a certiﬁcate of inspection issued by the American Lumber Standard Committee (ALSC) or the International Accreditation Service (IAS) accredited inspection agency. Inspection approval shall be marked on each piece. Shop drawings shall be submitted per subsection 105.02 for all major structures and for other structures when speciﬁed. The Department may provide an inspector at the treating plant for material quality review and inspection of the treatment process for treated timber. The plant shall notify the Engineer suﬃciently in advance of time of treating so that inspection may be arranged.

Revision of Section 607

Fences

Revise Section 607 of the Standard Specifications as follows:

Revise Subsection 607.01 and 607.02 as shown:

Description

607.01 This work consists of the construction of fence and gates, and removal of temporary plastic fence per these speciﬁcations and in conformity with the lines and grades shown on the plans or established.

Materials

607.02 Materials shall meet the requirements speciﬁed in the following subsections: Woven Wire 710.02 Barbed Wire 710.01 Chain Link Fabric 710.03 Fence Posts 710.07 Snow Fence 710.04 Timber for Wood Noise Barrier 710.06

Revision of Section 710

Fence and Guardrail

Revise Section 710 of the Standard Specifications as follows:

Revise Subsection 710.06 (4), and (5) as shown:

  - Timber for Wood Noise Barrier. Timber shall be any of the timber species given in subsection 508.02 including all species deﬁned as “Native.” Throughout the project, posts shall be of one species; boards may be of another species; and rails may be a mix of any permissible species, except where single sided fence is built, the rails shall be of one species. The exposed board surfaces shall be of one ﬁnish throughout the entire fence and may be rough sawn, SIS, S1S2E, or S48 S4S; posts and rails may have any of the ﬁnishes. Species selected for posts, rails, and boards shall conform to the grading rules of the Western Wood Products Association (WWPA), the Southern Pine Inspection Bureau (SPIB), or the West Coast Lumber Inspection Bureau (WCLIB) for grading and strength.

- Posts. WWPA or WCLIB posts and timbers, No. 1 or better; or SPIB timbers No. 2SR 2 or better.

- Rails. WWPA, WCLIB, or SPIB: Light framing, standard or better; or structural joists and planks, No. 2 or better.

- Boards. WWPA No. 2 common or better; or SPIB No. 1 or better.

- Treatment. The selected species shall be pressure treated lumber or timbers conforming in all respects to AASHTO M133, the AWPA Standard U1, Commodity Speciﬁcation A: Sawn Products UC4A and Section 508.04. AWPA Commodity Standard B: Posts (Ground contact for posts, above ground for balance of fence). A treatment report is required from the treatment plant. All posts and rails for noise barriers, and fence boards shall be dried after treatment to a maximum of 19 percent moisture content.

- Preservative. AASHTO M-133. [Note: moved to “(4) Treatment”, and other clariﬁcations.]

All lumber shall be manufactured per Product Standard 20-70 as published by the Department of Commerce and shall be grade marked by a grading agency or have an accompanying certiﬁcate from the grading agency. The grading agency shall be certiﬁed by the Board of Review of the American Lumber Standards Committee. All posts, rails, and fence board materials shall be dried after treatment to a maximum of 19 percent moisture content.

Revise Subsection 710.07 as shown:

  - Fence Posts, Rails and Gates. Round wood posts shall conform to the details and dimensions indicated on the plans. Wood posts and shall be straight, sound, and seasoned with ends sawed oﬀ square or as indicated. All knots shall be trimmed ﬂush with the surface. Wood posts shall be peeled and shall be treated with preservative per AASHTO M 133 or and AWPA Standards U1; Commodity Speciﬁcation B: Posts; UC4A . When native cedar posts are called for on the plans, the requirements for peeling and for treating may be omitted. A It Round posts shall be of the species and grades indicated on the plans.

When cedar split rail posts are called for on the plans, the requirements for peeling and for treating may be omitted.

All dimensional timber and lumber installed for fences and gates shall be sound, straight, and free from splits.

Revise and renumber previous Subsection 710.07 to 710.08, as shown:

  - Guardrail Posts and Blocks. Posts shall be of either wood or steel. When the choice of post is at the option of the Contractor, there shall be only one kind furnished on the project unless otherwise speciﬁed in the Contract.

(a) Wood posts and blocks shall meet the requirements of AASHTO M168, be fabricated from an approved or speciﬁed timber species and shall be of the quality, diameter or section, and length as speciﬁed or as shown on the plans in the Contract. Treated posts and blocks shall be fabricated or framed before treatment and shall conform to the requirements of AASHTO M 133 or and AWPA Standards U1; Commodity Specification A: Sawn Material; UC4B; and Section 508.04.