CDOT’s 2019 Field Materials Manual

CP-52 Contractor Asphalt Mix Design Approval Procedures

This materials bulletin replaces CP-52 of the 2019 Field Materials Manual.   The RAP aggregate bulk specific gravity will be back-calculated using an assumed average aggregate water absorption of 1.01%. The corresponding assumed aggregate asphalt absorption will be 0.61.  The corresponding CDOT Form # 429 has also been updated.

It is your responsibility as the owner of your 2019 Field Materials Manual to print these pages for replacement within your printed copy of the manual.  If you have questions, please contact Michael Stanford at 303-398-6576.

References:

All Material Bulletins can be found here: Materials Bulletins.