PERMANENT CHANGES TO PROJECT DATED SPECIAL PROVISIONS

**REVISION OF SECTION** 509 WELDING - EXISTING STEEL

DATE AUTHOR DESCRIPTION OF CHANGE

9/19/90 SHAMU MINOR CHANGES TO FORMAT

12/18/91 MAL Revised subsection references to conform with 1991 Specifications Book.

 This Special Provision is for the welding of existing steel. The Staff Materials Branch should be contacted to review the 509 Special Provisions on projects utilizing existing structural steel.

9/29/1999 M. Nord Verified the specification references for conformance with the *1999 Colorado DOT Standard Specifications for Road and Bridge Construction*.

 No exceptions were found.

 Converted to Microsoft Word 97 SR-2

04.11.2023 M. Kayen Revisions to make spec online ADA-compliant. 5.22.23 Additional ADA.

**Revise Section 509 of the Standard Specification for this project as follows:**

**Subsection 509.20 shall include the following:**

For field welding A7 steel, electrodes used shall be E7015, 16, 18, or 28.

For welding A7 steel with low-hydrogen electrodes by any process, the minimum preheat and interpass temperature shall be 150°F for thicknesses of metal up to 1-1/2 inches.

**Subsection 509.26 shall include the following:**

The Contractor shall not commence any field welding on the girders until the Division's Materials Branch has been notified and their inspector is on the site. The preheating process shall be approved by the Division's inspector.

**Subsection 509.20(h) shall include the following:**

Base metal shall be preheated to 150°F on the surface prior to welding studs.