# Revision of Section 208

# Sandbags

Revise Section 208 of the Standard Specifications for this project as follows:

Subsection 208.02 shall include the following:

- Sandbag.

Sandbags shall consist of woven polypropylene, polyethylene, or polyamide fabric with  a minimum fabric weight of four ounces per square yard:

Physical Requirements for Sandbag Geotextiles

| Property | Requirement | Test Method |
| --- | --- | --- |
| Mullen Burst | 300 psi | ASTM D3786 |
| Ultraviolet Resistance | 70% | ASTM D4355 |

Burlap is not an acceptable fabric; do not use it for sandbag material.

Sandbags shall consist of permeable material free from clay and harmful material.

Percent by Weight

Passing through Square Mesh Sieves

| Sieve Size | Percentage Passing |
| --- | --- |
| 3/8 in | 100% |
| No. 4 | 70-100% |

Permeable material shall have a sand equivalent value of not less than 75 percent.

Approve fill material before installation.

Sandbags shall meet the following requirements for size and weight:

Minimum Dimensions

| Dimensions (Nominal) inches | Weight-Minimum |
| --- | --- |
| 18 (Length) x 12 (Width) x 3 (thickness) | 33 lb |

Approve size and weight substitutions before installation.

Subsection 208.11 shall include the following:

Measure sandbags by the actual linear feet installed and accepted.

Subsection 208.12 shall include the following:

Pay 	 Item			Pay Unit

Sandbag				Linear Foot