# Revision to Section 522

# Environmental Stain (Galvanized)

Add Section 522 to the Standard Specifications to include the following:

Subsection 522.01 shall include the following:

This work consists of applying an environmentally and wildlife safe, non-caustic, non-pigment-based surface stain to all visible galvanized steel surfaces, including galvanized steel supports.

Subsection 522.02 shall include the following:

(h)	Environmental surface stain shall consist of a clear, soluble solution of natural elements and soft-buffered organic acids. No pigment-based colorants shall be added to achieve the desired color. The stain shall react with the target surface over 7 to 21 days to produce consistent color and matte finish specified on the plans or approved by the Engineer. The stain shall be resistant to fading in the sun and have a minimum life expectancy of 25 years.

Submit a copy of the manufacturer's product Safety Data Sheet for all related products (including cleaning agents) together with instructions for application of stain, a minimum of 5 days before staining the sample section. Submit proposed methods to control overspray, spillage, and protection of adjacent surfaces in writing for approval.  Do not begin staining until written approval has been received.

- Stain Sample.  Apply stain to a minimum 12-inch sample section of galvanized metal. If staining occurs on-site, stain the sample in the presence of the Engineer. Notify the Engineer a minimum of 7 days before staining the sample section. Prepare and stain the sample section with the same materials, tools, equipment, and methods used in staining final surfaces. Allow the applied stain to cure for a minimum of 21 days. Submit the sample to the Engineer for approval. The cost of materials and labor necessary to achieve the accepted sample shall be included in the price of the work. If more than one sample section is required, include each additional sample in the work price. Use the approved sample as the standard of comparison in determining the acceptability of staining.

- Stain Application.  Before applying the stain onto the metal surface, clean excessive oils, dirt, and other contaminants with cleaning agents conforming to the manufacturer’s recommendations and approval.  All surfaces shall be dry before applying the stain. Apply all stain per manufacturer′s recommendations to achieve color consistent with the approved sample.

If spray application is used, follow the manufacturer’s recommendations. Minimize overspray on undesired surfaces and protect adjacent surfaces from overspray. Do not perform spray application under windy or rainy conditions. Apply stain uniformly, free from sags, runs, or defects of any kind. Correct irregularities according to the stain manufacturer′s recommendations.  Keep stained surfaces dry for a period of 5 days following the application of stain.

If immersion application is used, immerse the structure in a controlled area following the manufacturer’s recommendations. Minimize splashing, dripping, and runoff on surfaces not intended for stain application. The structure shall have a uniform appearance, free from sags, runs, or defects of any kind. Correct irregularities according to the manufacturer′s recommendations. Keep stained surfaces dry for a period of 5 days following the application of stain.

Per the manufacturer’s recommendations, multiple applications, may be required to achieve the color of the approved stain sample.

Final approval of products will occur when the stain has achieved the color of the approved stain sample.

The Engineer will reject all substandard items not achieving the color of the approved stain sample.

- Storage of Materials.  Store stained surfaces properly at the construction yard after delivery, before, and up to the time of installation.  Place spacers between rows to allow for necessary airflow if components stack, for example, guardrail.  Stack items perpendicular to the ground slope to allow for proper drainage. Elevate items so they do not come into direct contact with soil or plant matter.  Conform to other standard storage procedures and manufacturer recommendations regarding storage.  Ensure all components are stored properly on site.

Subsection 522 Method of Measurement and Basis of Payment shall include the following:

Include all costs associated with applying environmental stain to galvanized steel surfaces, including multiple applications, cleaning surfaces, and preparing stain samples in the work. Do not measure and pay for them separately.