REVISION OF SECTION 614

SIGN PAINTING (MOCHA BROWN)

Section 614 of the Standard Specifications is hereby revised for this project as follows:

In subsection 614.09, eleventh paragraph, delete the first sentence and replace with the following:

Structural steel shall be given one shop coat of primer and 2 coats of mocha brown paint in conformity with subsection 509.24.  Mocha brown paint shall be manufactured to meet Fed. Spec. TT-E-529G and the color shall match Fed. Std. 595a, No. 10075.  All exposed portions of galvanized steel shall conform to the following:

(a)	All foreign substances shall be removed.

(b)	One coat of bonding agent shall be applied uniformly on the surface.  Bonding agent shall be Vinyl Butyral Wash Primer conforming to MIL-P-15328 (SSPC Paint No. 57).  After the bonding agent has dried sufficiently, (not more than 24 hours) one coat of exterior enamel shall be applied by a suitable method that will insure a uniform coating free of blemishes, discontinuities, bare edges or other imperfections.  Defective surfaces shall be touched up with paint as required.

Structural members, walkway grating, brackets, railing, electrical conduit, metal sign posts, backing zees and the backside of all new sign panels, for signs indicated in the Tabulation of Signs and Overhead Sign Tabulation, shall be painted mocha brown.  Paint shall conform to Section 708.  All aluminum surfaces to be painted shall be prepared as noted above for galvanized steel.

Subsection 614.14 shall include the following:

Painting signs and sign structures mocha brown will not be paid for separately but shall be included in the work.